## Slide 1: Failure Modes and Theories of Laminated CFRP
By Dr. Mahdi Damghani

## Slide 2: Failure modes- Introduction
Basic mechanisms of laminate failure are:
  Longitudinal fracture of matrix
  Transverse matrix fracture
  Fibre-matrix debonding
  Fibre fracture
  Delamination
Shear stress in the matrix reaches matrix shear strength
Tensile stress in the matrix reaches matrix tensile strength
Debonding stress is higher than shear strength of the matrix
Notes: Intro “This slide explains the main ways a composite laminate can fail. Knowing these failure modes helps engineers understand why damage starts and how to design stronger, safer composite parts.”
Concept Composite materials can fail in several ways depending on how the load is applied and how well the fibres and matrix work together:
Longitudinal matrix fracture happens when the shear stress in the matrix becomes too high, causing cracks that run along the fibres.
Transverse matrix fracture occurs when tension across the fibres is greater than what the matrix can handle, creating cracks that cut across the fibre direction.
Fibre–matrix debonding occurs when the bond between the fibre and matrix breaks, meaning the load can no longer transfer properly between them.
Fibre fracture takes place when the fibres themselves snap because the stress is higher than their strength.
Delamination is when layers of the laminate separate from each other, usually from out-of-plane stresses or impact.
Details The figures show how each failure mode looks inside a laminate. The cracks can start in the matrix (either along or across the fibres), at the interface (debonding), or within the fibres themselves. Delamination usually spreads between layers and can grow over time with repeated loading. In real components, these failures often happen together, leading to progressive damage that reduces stiffness and strength before total failure.
Key Takeaway Composite laminates don’t usually fail in a single way. Instead, several damage mechanisms interact — cracks form, fibres break, layers separate — and this progressive failure defines how the material behaves under real service loads. Understanding each mode helps engineers predict failure and design more damage-tolerant structures.

## Slide 3: Fracture modes- Example 1
The fracture mechanism depends on:
  The nature of constituents
  The architecture of the layer
  Mode of mechanical loading
For example, for a cross-ply laminate subject to tensile loading:
  Longitudinal fracture of the matrix and/or fracture at the fibre-matrix interface in the layers oriented at 90°
  Fracture of the fibres in the layers at 0°
  The transverse fracture of the matrix in the layers at 0°
Side view of fracture of a [0/90]2s CFRP with a hole at the centre showing transverse fracture of 90o plies.
Half the laminate is shown
Notes: Intro “This slide gives an example of how different failure modes appear in a cross-ply laminate. It shows how the stacking sequence, materials, and type of loading combine to control where and how damage begins.”
Concept The way a composite laminate fractures depends on three main factors:
Nature of constituents: the stiffness and strength of the fibres and matrix.
Layer architecture: fibre orientation and ply stacking (e.g., 0°/90° cross-ply).
Mechanical loading: whether the stress is tensile, compressive, or shear.
For a cross-ply laminate under tensile loading, the sequence of damage typically follows this pattern:
Longitudinal fracture of the matrix or cracking along the fibre–matrix interface in the 90° plies, where stress concentrations are high.
Fibre fracture in the 0° plies as the load increases and the fibres reach their tensile limit.
Transverse matrix cracking in the 0° layers, completing the failure process.
Details The top schematic shows alternating 0° and 90° plies, half of the laminate for simplicity. The micrograph displays a side view of a [0/90]₂ₛ carbon fibre reinforced polymer (CFRP) specimen with a central hole—an intentional stress raiser. The 90° plies exhibit transverse matrix cracking initiated by local tensile stresses around the hole, while the 0° plies carry most of the load until fibre fracture occurs. These progressive events demonstrate how ply orientation controls damage evolution in multi-directional laminates.
Key Takeaway In cross-ply CFRP laminates, fracture begins in the weaker 90° plies through matrix cracking and debonding, then progresses to fibre failure in the 0° plies. The overall fracture pattern is strongly influenced by fibre orientation and local stress concentrations such as holes or notches.

## Slide 4: Fracture modes- Example 2
For example, for an angle-ply laminate subject to tensile loading:
  The longitudinal matrix fracture in the ±45° layers
  Delamination between layers
Half the laminate is shown
Notes: Intro “This slide shows how fracture develops in an angle-ply laminate. The example helps visualise how off-axis fibre orientations affect both the direction and type of damage under tension.”
Concept When an angle-ply laminate (such as ±45°) is stretched, the fibres are not aligned with the loading direction, so the matrix carries a larger share of the shear load. Two main failure modes appear:
Longitudinal matrix fracture along the ±45° fibre directions, caused by high shear stress between fibres and matrix.
Delamination between layers, where cracks from one ply grow into neighbouring plies with opposite orientation, leading to layer separation.
Details The schematic shows alternating ±45° plies in half of the laminate. The experimental image reveals diagonal cracks following fibre paths in the ±45° layers—evidence of matrix shear failure. As these cracks grow, they reach the ply interfaces, where mismatched orientations and interlaminar stresses trigger delamination. This is typical of angle-ply laminates because the fibres’ off-axis alignment transfers load through shear rather than direct tension, making the matrix–interface regions more vulnerable.
Key Takeaway In angle-ply laminates, failure is dominated by shear-driven matrix cracking and delamination. The ±45° fibre orientation promotes diagonal crack growth and layer separation, showing how ply angle directly controls the failure pattern and load-carrying efficiency of composite laminates.

## Slide 5: Fracture modes- Example 3
For example, for a Quasi-isotropic ply laminate subject to tensile loading:
  First, longitudinal cracking of the matrix is induced in the 90° layers
  Matrix cracking is initiated in the ±45° layers from the cracks propagated in the 90° layers with a limited propagation of the cracks at ±45°
  Initiation of longitudinal matrix cracks initiated from the hole, which propagate in the 0° layers
  These cracks also generate secondary cracks in ±45° layers
  In the last stage, the longitudinal cracks in 0° layers induce a delamination of the layers followed by the fracture of 90° layers, then of ±45°, and lastly by the fracture of fibres in 0° layers, leading to the final fracture of the plate
Notes: Intro “This slide illustrates how a quasi-isotropic laminate fails under tensile loading. Because it includes plies at 0°, ±45°, and 90°, it shows a progressive and complex failure pattern similar to that seen in real composite aircraft components.”
Concept
Quasi-isotropic laminates have plies in multiple orientations (0°, ±45°, 90°), giving nearly equal in-plane stiffness in all directions.
Under tensile loading, different plies fail at different stages due to varying stress states:
  90° plies fail first through matrix cracking.
  ±45° plies fail next as cracks spread through shear.
  0° plies carry the most load and fail last by fibre fracture.
The failure process is sequential and highly dependent on the interaction between layers.
Details
The 90° plies develop longitudinal matrix cracks first, especially near holes or notches where stresses are highest.
These cracks extend into the ±45° plies, causing limited shear cracking.
Longitudinal cracks then appear in the 0° plies, starting from stress concentrations at the hole edges.
Secondary cracking forms in the ±45° plies, and delamination begins between layers.
Final failure occurs as delamination spreads and the 0° fibres fracture, leading to total laminate separation.
The diagrams show this step-by-step progression: 90° cracking (yellow), ±45° cracking (blue), and finally 0° cracking (purple).
Key Takeaway
Quasi-isotropic laminates fail progressively, starting with matrix cracking in 90° plies and ending with fibre breakage in 0° plies.
Each ply orientation plays a distinct role in damage evolution, making the sequence of failure predictable but complex.
Understanding this sequence helps engineers design balanced laminates that delay catastrophic failure and maintain load capacity even after initial cracking.

## Slide 6: Failure modes- Unidirectional composite subjected to longitudinal tension
: The initiation of a fracture is generally produced either by fracture of fibres, when the fracture strain of the fibres is less than that of the matrix or by transverse matrix fracture in the opposite case.
Ultimate stress of the composite
Stress in matrix at strain equal to the ultimate strain of the fibres
Volume fraction
Ultimate stress of the matrix
Stress in the fibre at strain equal to the ultimate strain of the matrix
The matrix does not allow us to benefit from the fibre reinforcement
Notes: Intro “This slide explains how a unidirectional composite behaves when it is pulled along the fibre direction. It shows how the relative strength and strain capacity of fibres and matrix determine whether failure begins in the matrix or the fibres.”
Concept
Unidirectional composites are designed so that fibres carry most of the load along their length, with the matrix transferring stress between fibres.
The overall composite strength depends on both constituent strengths and their volume fractions (Vf for fibres, Vm = 1–Vf for matrix).
Two main cases define the failure behaviour:
  Case 1: Fibre strain at failure (εfu) < Matrix strain at failure (εmu) → Fibres break first.
  Case 2: Fibre strain at failure (εfu) > Matrix strain at failure (εmu) → Matrix cracks first.
Details
Case 1 (εfu < εmu):
  Typical for stiff, brittle fibres (e.g., carbon).
  Fibres reach their fracture strain first, causing composite failure even though the matrix can still deform.
  The composite’s ultimate stress (σcu) ≈ σfu × Vf, meaning failure strength scales with fibre strength and volume fraction.
Case 2 (εfu > εmu):
  Common for ductile fibres (e.g., glass or aramid) in a brittle matrix.
  The matrix cracks first when its tensile strain limit is exceeded, preventing full fibre reinforcement benefit.
  The composite fails at lower stress since the load can no longer transfer effectively through the cracked matrix.
The stress–strain plots show that the composite behaviour lies between the individual fibre and matrix curves. The slope (modulus) and ultimate stress are controlled by fibre content and relative strain limits.
Key Takeaway
Whether a unidirectional composite fails by fibre fracture or matrix cracking depends on which constituent reaches its strain limit first.
For carbon/epoxy systems, fibres usually fail first; for glass or aramid composites, matrix cracking dominates.
Designing effective composites means matching fibre and matrix properties to balance stiffness, strength, and strain capacity for the intended load direction.

## Slide 7: Failure modes- Unidirectional composite subjected to longitudinal tension
For carbon fibres:
  High Strength (HS)
  High Modulus (HM)
For E-glass fibres:
Typical resins:
Notes: Intro “This slide presents typical mechanical properties of carbon and glass fibres, as well as common resin systems. Comparing their stiffness, strength, and strain-to-failure helps predict which constituent will fail first when the composite is loaded in tension.”
Concept
Fibre type determines both strength and stiffness of the composite.
Matrix type governs ductility and strain-to-failure.
The balance between fibre and matrix properties defines whether the composite behaves in a brittle or ductile manner under longitudinal tension.
Details
Carbon fibres:
  High Strength (HS):
  High Modulus (HM):
  Carbon fibres are very stiff and strong but have low strain capacity, so they tend to fracture before the matrix (εfu < εmu).
E-glass fibres:
  These fibres are more ductile than carbon and can stretch beyond the matrix limit (εfu > εmu), so matrix cracking occurs first.
Typical resin matrices:
  Rigid polyesters:
  Phenolic resins:
  Epoxy resins:
  Resins are relatively ductile but much weaker and less stiff than fibres; their role is mainly load transfer and crack resistance.
Key Takeaway
High-strength carbon fibres fail before the matrix (brittle response).
E-glass fibres outlast the matrix in strain (ductile response).
Choosing fibre and resin combinations with compatible strain limits ensures balanced and predictable composite behaviour under longitudinal tension.
Intro “This slide presents typical mechanical properties of carbon and glass fibres, as well as common resin systems. Comparing their stiffness, strength, and strain-to-failure helps predict which constituent will fail first when the composite is loaded in tension.”
Concept
Fibre type determines both strength and stiffness of the composite.
Matrix type governs ductility and strain-to-failure.
The balance between fibre and matrix properties defines whether the composite behaves in a brittle or ductile manner under longitudinal tension.
Details
Carbon fibres:
  High Strength (HS):
    𝐸_𝑓=220" GPa"
    𝜎_𝑓𝑢=3000"–" 4000" MPa"
    𝜀_𝑓𝑢=1.4"–" 1.8%
  High Modulus (HM):
    𝐸_𝑓=400" GPa"
    𝜎_𝑓𝑢=2200" MPa"
    𝜀_𝑓𝑢=0.5%
  Carbon fibres are very stiff and strong but have low strain capacity, so they tend to fracture before the matrix (εfu < εmu).
E-glass fibres:
  𝐸_𝑓=70" GPa"
  𝜎_𝑓𝑢=2400"–" 3400" MPa"
  𝜀_𝑓𝑢=3.4"–" 4.8%
  These fibres are more ductile than carbon and can stretch beyond the matrix limit (εfu > εmu), so matrix cracking occurs first.
Typical resin matrices:
  Rigid polyesters: 𝜀_𝑚𝑢=2"–" 5%
  Phenolic resins: 𝜀_𝑚𝑢=2.5%
  Epoxy resins: 𝜀_𝑚𝑢=2"–" 5%
  Resins are relatively ductile but much weaker and less stiff than fibres; their role is mainly load transfer and crack resistance.
Key Takeaway
High-strength carbon fibres fail before the matrix (brittle response).
E-glass fibres outlast the matrix in strain (ductile response).
Choosing fibre and resin combinations with compatible strain limits ensures balanced and predictable composite behaviour under longitudinal tension.

## Slide 8: Failure modes- Unidirectional composite subjected to longitudinal tension- Fracture propagation of high fibre-matrix bonding
Initiation by fracture of either the fibre or the matrix.
High stress region near the tip of the crack that leads to successive propagation of the fracture in the fibres and the matrix.
Brittle fracture
Bridging is observed by longitudinal fracture of the matrix and by fibre-matrix debonding, of two cracks initiated in different zones.
Notes: Intro “This slide illustrates how cracks grow in a unidirectional composite when the fibre–matrix bond is strong. It shows the step-by-step development of fracture under longitudinal tension and explains how high interfacial bonding influences failure behaviour.”
Concept
In composites with strong fibre–matrix bonding, cracks cannot easily deflect or stop at the interface.
As a result, stress concentrates at the crack tip, and fracture propagates directly through both matrix and fibres.
The process involves several stages:
  Crack initiation in either the fibre or the matrix.
  Rapid crack growth through high-stress regions near the crack tip.
  Possible fibre–matrix debonding or bridging between multiple cracks.
Details
Stage 1: Fracture starts in either the fibre or the matrix, usually at a weak spot or defect.
Stage 2: High local stress at the crack tip drives further propagation through the surrounding material.
Stage 3: Brittle fracture develops, with cracks spreading quickly across the load path.
Stage 4: In some regions, bridging occurs — cracks in different zones connect through longitudinal splitting and limited fibre–matrix debonding.
Strong bonding limits energy absorption because cracks do not easily deflect along the interface, producing a clean, brittle fracture surface.
Key Takeaway
High fibre–matrix bonding increases stiffness and load transfer efficiency but reduces toughness.
Cracks in such systems propagate rapidly and directly through both phases, resulting in a brittle failure mode.
Optimising the interfacial bond is key: too strong leads to brittle fracture, too weak causes premature debonding and strength loss.

## Slide 9: Failure modes- Unidirectional composite subjected to longitudinal tension- Fracture propagation of poor fibre-matrix bonding
Near the tip of the crack, the region of high stresses induces shear fracture of the fibre-matrix interface.
The crack propagates transversely to the fibres without fracture of fibres.
Behind the crack's tip, the crack opening induces high tension stresses in the fibres bridging the crack planes.
These high-tension stresses lead to the fracture of fibres at a distance next to the crack planes.
As the crack continues to propagate, the broken fibres are pulled out of the matrix.
Notes: Intro “This slide explains how cracks grow in a unidirectional composite when the fibre–matrix bonding is poor. It contrasts with the previous case by showing a more gradual and energy-absorbing failure process involving debonding and fibre pull-out.”
Concept
Poor interfacial bonding means the matrix cannot transfer stress efficiently to the fibres.
Cracks propagate mainly along the fibre–matrix interface, not through the fibres themselves.
The process involves progressive debonding, fibre pull-out, and delayed fibre fracture, which increases toughness but reduces stiffness and strength.
Details
At the crack tip, high local stresses produce shear fracture along the interface, causing the fibres to separate from the matrix without breaking.
The crack then moves transversely to the fibres, bypassing them rather than cutting through.
Behind the crack tip, tensile stresses develop in the bridging fibres, which resist opening of the crack.
As the load rises, these fibres eventually fracture some distance behind the crack front, and their broken ends are pulled out of the matrix.
The figure shows this progression—starting with debonding, followed by crack advance, fibre breakage, and pull-out.
Key Takeaway
Poor fibre–matrix bonding results in a more ductile and energy-dissipative failure mode through debonding and fibre pull-out.
This mechanism improves toughness but significantly lowers stiffness and tensile strength compared to composites with strong interfacial bonding.
Balancing interfacial strength is crucial: enough to transfer load effectively, but weak enough to allow controlled energy absorption through fibre pull-out.

## Slide 10: Failure modes- Unidirectional composite subjected to longitudinal tension- Fracture surfaces of poor fibre-matrix bonding
In some cases, on reaching the fibre-matrix interface the crack can split and propagate along the fibres.
Thus, different types of fracture surfaces can be observed, with a brush aspect of the crack surfaces.
Bridging is evident
Multiple bridging is evident
Notes: Intro “This slide shows the characteristic fracture surfaces of unidirectional composites when fibre–matrix bonding is poor. It highlights how cracks split, bridge, and form stepped or brush-like patterns rather than clean fractures.”
Concept
Poor bonding between fibre and matrix leads to interfacial crack splitting instead of through-fibre fracture.
The crack path follows the fibre–matrix interface, resulting in bridging and multiple step formations.
These surfaces reflect energy-dissipative failure, where fibres pull out and bridge across cracks, slowing propagation.
Details
When the advancing crack reaches the fibre–matrix interface, it can split and run parallel to the fibres.
This produces a brush-like appearance on the fracture surface due to partial fibre pull-out.
Bridging zones appear where intact fibres span across the crack, maintaining some load transfer.
With continued loading, multiple bridging regions develop, giving a stepped or serrated fracture pattern.
Such surfaces indicate that failure occurred by interfacial debonding rather than clean fibre breakage, showing that the interface absorbed part of the fracture energy.
Key Takeaway
Poor fibre–matrix bonding leads to rough, stepped fracture surfaces with clear evidence of fibre bridging and pull-out.
These features indicate enhanced toughness but reduced stiffness and strength.
Understanding these surface features helps diagnose interfacial quality in composite testing and failure analysis.

## Slide 11: Failure modes- Unidirectional composite subjected to transverse tension
  Fracture is produced either by matrix fracture or by debonding of the fibre-matrix interface.
  Matrix fracture is produced when the tensile stress in the matrix reaches the ultimate stress of the matrix.
  This process occurs when the fracture stress of the matrix is lower than the tensile debonding stress of the fibre-matrix.
  The fracture of the composite is governed by the fibre-matrix interface.
Notes: Intro “This slide explains how a unidirectional composite behaves under transverse tension, where the applied load is perpendicular to the fibres. The failure mode depends on whether the matrix or the fibre–matrix interface is weaker.”
Concept
Transverse tension primarily loads the matrix and the fibre–matrix interface, not the fibres themselves.
Two main cases determine the mode of failure:
  : The matrix fails first because its tensile strength is lower than the interface debonding stress.
  : The interface fails first, leading to fibre–matrix debonding.
Details
When :
  The matrix cracks once the applied tensile stress equals its ultimate strength .
  Cracks propagate through the resin-rich regions between fibres, often forming perpendicular to the loading direction.
  The figure shows a clean transverse matrix crack, typical of brittle polymers like epoxies.
When :
  The fibre–matrix interface debonds first because it cannot sustain the tensile stress transferred from the matrix.
  This causes interfacial cracking and local stress redistribution around fibres.
  The lower image depicts this interfacial failure pattern, which is less brittle but leads to reduced stiffness.
Key Takeaway
Under transverse tension, unidirectional composites fail either by matrix cracking or interface debonding, depending on which constituent is weaker.
The matrix-dominated direction has low tensile strength, making it a common site for microcrack initiation in service.
Enhancing transverse strength requires improving matrix toughness and interface adhesion without compromising flexibility.
Intro “This slide explains how a unidirectional composite behaves under transverse tension, where the applied load is perpendicular to the fibres. The failure mode depends on whether the matrix or the fibre–matrix interface is weaker.”
Concept
Transverse tension primarily loads the matrix and the fibre–matrix interface, not the fibres themselves.
Two main cases determine the mode of failure:
  𝜎_𝑚𝑢<𝜎_𝑑: The matrix fails first because its tensile strength is lower than the interface debonding stress.
  𝜎_𝑚𝑢>𝜎_𝑑: The interface fails first, leading to fibre–matrix debonding.
Details
When 𝜎_𝑚𝑢<𝜎_𝑑:
  The matrix cracks once the applied tensile stress equals its ultimate strength 𝜎_𝑚𝑢.
  Cracks propagate through the resin-rich regions between fibres, often forming perpendicular to the loading direction.
  The figure shows a clean transverse matrix crack, typical of brittle polymers like epoxies.
When 𝜎_𝑚𝑢>𝜎_𝑑:
  The fibre–matrix interface debonds first because it cannot sustain the tensile stress transferred from the matrix.
  This causes interfacial cracking and local stress redistribution around fibres.
  The lower image depicts this interfacial failure pattern, which is less brittle but leads to reduced stiffness.
Key Takeaway
Under transverse tension, unidirectional composites fail either by matrix cracking or interface debonding, depending on which constituent is weaker.
The matrix-dominated direction has low tensile strength, making it a common site for microcrack initiation in service.
Enhancing transverse strength requires improving matrix toughness and interface adhesion without compromising flexibility.

## Slide 12: Failure criteria- Introduction
Laminated Carbon Fibre Reinforced Polymer (CFRP) and Glass Fibre Reinforced Polymers (GFRP) are brittle materials:
  The failure is abrupt with sudden burst of energy not showing signs of plasticity or yielding as seen in conventional metallic materials.
For ductile materials (aluminum, titanium, steel, etc), the failure criteria are described by:
  Von Mises (alternative names: Maxwell-Huber-Hencky, distortion energy or octahedral shear stress) yield criterion.
  Tresca (alternative names: maximum shear stress or otherwise known as Guest) yield criterion.
  Mohr-Coulomb criterion.
  Drucker-Prager criterion.
In the next two slides, the failure criteria for ductile material are presented for information only (beyond the scope of this lecture).
Notes: Intro “This slide introduces the concept of failure criteria, distinguishing between brittle and ductile materials. It explains why composite materials such as CFRP and GFRP fail suddenly without yielding, unlike metals that deform plastically before fracture.”
Concept
Composites (CFRP, GFRP) behave as brittle materials:
  Failure is abrupt, with little or no plastic deformation.
  There is no yielding phase—failure occurs when the maximum stress exceeds the material’s limit.
  Energy absorption is low, represented by the small area under the stress–strain curve.
Ductile materials (e.g., aluminium, titanium, steel) exhibit:
  Gradual yielding and plastic deformation before fracture.
  Larger energy absorption due to significant strain hardening.
  Predictable behaviour defined by yield criteria.
Details
For ductile materials, the following classical failure criteria apply:
  Von Mises criterion – also known as Maxwell–Huber–Hencky or octahedral shear stress theory; based on distortion energy.
  Tresca criterion – also called the maximum shear stress or Guest yield criterion; simpler but more conservative.
  Mohr–Coulomb and Drucker–Prager criteria – used for pressure-dependent or frictional materials (e.g., soils, polymers).
The plot compares brittle vs ductile stress–strain behaviour:
  Brittle materials show sharp fracture near the elastic limit.
  Ductile materials exhibit extended plastic deformation before failure.
  The area under the curve represents the energy absorbed prior to failure—large for ductile metals, small for composites.
Key Takeaway
CFRP and GFRP laminates are brittle—they fail suddenly without yielding.
Metals are ductile, showing visible plastic deformation before failure.
Understanding this contrast is crucial: composites require failure criteria based on strength rather than yield, unlike metals that rely on plastic flow theories.

## Slide 13: Failure criteria- Ductile material
Von Mises vs Tresca (3D)
Von Mises vs Tresca (2D)
Maximum shear stress reaches the Yield stress for shear of the material in tensile test (0.5).
and are maximum and minimum principal stresses.
Failure occurs when octahedral shear stress is equal to the octahedral shear stress at yield.
Notes: Intro “This slide compares the Von Mises and Tresca yield criteria for ductile materials, explaining how each predicts the onset of yielding under multi-axial stress states. Both are essential for metals but not applicable to brittle materials like composites.”
Concept
Von Mises criterion:
  Yielding begins when the distortion energy in a material reaches the same value as in a uniaxial tension test at yield.
  It assumes yielding is independent of hydrostatic stress (no effect from pure pressure).
  Expressed as:
Tresca criterion:
  Yielding occurs when the maximum shear stress equals the shear stress at yield in a simple tension test.
  Expressed as:
Both criteria describe yielding for ductile materials like steel, aluminium, and titanium alloys but predict slightly different yield surfaces.
Details
In 3D stress space, the Von Mises surface is a smooth cylinder, while the Tresca surface is a hexagonal prism—Tresca is more conservative (predicts earlier yield).
In 2D, both appear as curves in the σ₁–σ₂ plane:
  Von Mises → elliptical shape (distortion energy).
  Tresca → hexagonal shape (maximum shear).
The octahedral shear stress (τₒct) describes yielding when distortion energy equals that at yield:
where is the second invariant of the deviatoric stress tensor.
These criteria help engineers predict failure in complex stress states (pressure vessels, shafts, thin-walled structures).
Key Takeaway
Von Mises gives a smooth, accurate prediction of ductile yielding; Tresca offers a simpler, more conservative approximation.
Both apply only to ductile materials capable of plastic deformation—not to composites, which fail by fracture rather than yield.
Understanding these criteria provides a foundation for appreciating why composite failure theories use strength-based, not yield-based, formulations.
Intro “This slide compares the Von Mises and Tresca yield criteria for ductile materials, explaining how each predicts the onset of yielding under multi-axial stress states. Both are essential for metals but not applicable to brittle materials like composites.”
Concept
Von Mises criterion:
  Yielding begins when the distortion energy in a material reaches the same value as in a uniaxial tension test at yield.
  It assumes yielding is independent of hydrostatic stress (no effect from pure pressure).
  Expressed as:
√((𝜎_1−𝜎_2 ├ )┤^2+(𝜎_2−𝜎_3 ├ )┤^2+(𝜎_3−𝜎_1 ├ )┤^2 ┤┤┤/2)=𝜎_𝑦𝑠
Tresca criterion:
  Yielding occurs when the maximum shear stress equals the shear stress at yield in a simple tension test.
  Expressed as:
Both criteria describe yielding for ductile materials like steel, aluminium, and titanium alloys but predict slightly different yield surfaces.
Details
In 3D stress space, the Von Mises surface is a smooth cylinder, while the Tresca surface is a hexagonal prism—Tresca is more conservative (predicts earlier yield).
In 2D, both appear as curves in the σ₁–σ₂ plane:
  Von Mises → elliptical shape (distortion energy).
  Tresca → hexagonal shape (maximum shear).
The octahedral shear stress (τₒct) describes yielding when distortion energy equals that at yield:
𝜏_𝑜𝑐𝑡=1/3 √(2𝐽_2 )
where 𝐽_2is the second invariant of the deviatoric stress tensor.
These criteria help engineers predict failure in complex stress states (pressure vessels, shafts, thin-walled structures).
Key Takeaway
Von Mises gives a smooth, accurate prediction of ductile yielding; Tresca offers a simpler, more conservative approximation.
Both apply only to ductile materials capable of plastic deformation—not to composites, which fail by fracture rather than yield.
Understanding these criteria provides a foundation for appreciating why composite failure theories use strength-based, not yield-based, formulations.

## Slide 14: Failure criteria- Ductile material
Drucker-Prager
and are yield stresses under tension and compression.
Drucker-Prager vs Mohr-Coulomb
Principal stresses
Notes: Intro “This slide introduces the Drucker–Prager failure criterion, an extension of the Von Mises model that incorporates the effect of hydrostatic pressure. It is particularly useful for pressure-sensitive, ductile, or frictional materials such as soils, polymers, and some metals under complex stress states.”
Concept
The Drucker–Prager criterion generalises Von Mises by including the influence of mean (hydrostatic) stress on yielding.
It assumes that yielding depends on both:
  Deviatoric stress (shear-related distortion, ).
  Hydrostatic stress (pressure, ).
The criterion is expressed as:
where and is the second invariant of the deviatoric stress tensor.
Details
The parameters and are material constants derived from tensile () and compressive () yield stresses:
Geometrically, the Drucker–Prager surface is a smooth cone in principal stress space, enclosing the hexagonal Mohr–Coulomb surface.
The figure shows that Drucker–Prager offers a convenient, differentiable approximation of Mohr–Coulomb behaviour.
The model predicts that yielding depends on both shear and pressure, making it suitable for non-metallic ductile materials that show different strengths in tension and compression (e.g., concrete, polymers, certain adhesives).
Key Takeaway
The Drucker–Prager criterion accounts for the effect of hydrostatic pressure, unlike Von Mises or Tresca.
It bridges the gap between metallic yield models (pressure-insensitive) and frictional materials (pressure-sensitive).
This approach underpins modern constitutive models for polymers, soils, and composite matrices, especially under combined tension and compression.
Intro “This slide introduces the Drucker–Prager failure criterion, an extension of the Von Mises model that incorporates the effect of hydrostatic pressure. It is particularly useful for pressure-sensitive, ductile, or frictional materials such as soils, polymers, and some metals under complex stress states.”
Concept
The Drucker–Prager criterion generalises Von Mises by including the influence of mean (hydrostatic) stress on yielding.
It assumes that yielding depends on both:
  Deviatoric stress (shear-related distortion, 𝐽_2).
  Hydrostatic stress (pressure, 𝐼_1).
The criterion is expressed as:
𝑓(𝐼_1ⓜ,𝐽_2 )=𝛼𝐼_1+√(𝐽_2 )−𝑘=0
where 𝐼_1=𝜎_1+𝜎_2+𝜎_3and 𝐽_2is the second invariant of the deviatoric stress tensor.
Details
The parameters 𝛼and 𝑘are material constants derived from tensile (𝜎_𝑡) and compressive (𝜎_𝑐) yield stresses:
𝛼=1/√3 ((𝜎_𝑡−𝜎_𝑐)/(𝜎_𝑐+𝜎_𝑡 )), 𝑘=2/√3 ((𝜎_𝑐 𝜎_𝑡)/(𝜎_𝑐+𝜎_𝑡 ))
Geometrically, the Drucker–Prager surface is a smooth cone in principal stress space, enclosing the hexagonal Mohr–Coulomb surface.
The figure shows that Drucker–Prager offers a convenient, differentiable approximation of Mohr–Coulomb behaviour.
The model predicts that yielding depends on both shear and pressure, making it suitable for non-metallic ductile materials that show different strengths in tension and compression (e.g., concrete, polymers, certain adhesives).
Key Takeaway
The Drucker–Prager criterion accounts for the effect of hydrostatic pressure, unlike Von Mises or Tresca.
It bridges the gap between metallic yield models (pressure-insensitive) and frictional materials (pressure-sensitive).
This approach underpins modern constitutive models for polymers, soils, and composite matrices, especially under combined tension and compression.

## Slide 15: Failure criteria- Brittle composites
2D stress state:
  Unidirectional CFRP/GFRP
    Maximum stress failure theory
    Maximum strain failure theory
    Tsai-Hill
    Hoffman
    Tsai-Wu
    Hashin-Rotem
    Puck
    Yamada Sun
    LaRC03
2D stress state:
  Bi-directional CFRP/GFRP (woven)
    See the opposite paper:
    Chang-chang
    Puck
3D stress state:
  Modification of the abovementioned criteria (3D Hashin, Yamada Sun)
  3D Puck
Notes: Intro “This slide summarises the main failure criteria used for brittle composite materials such as CFRP and GFRP. Unlike ductile metals, composites fail without yielding, so their failure prediction is based on stress or strain limits within the laminate.”
Concept
Brittle composite laminates (CFRP, GFRP) are analysed using strength-based criteria, not yield theories.
These criteria relate applied stresses or strains to the material’s strength in different directions—fibre, matrix, and shear.
Models differ based on laminate type and stress state:
  2D stress state: in-plane loading for unidirectional or woven laminates.
  3D stress state: through-thickness stresses and interlaminar effects.
Details
For unidirectional CFRP/GFRP (2D):
  Maximum stress theory – failure occurs when any stress component exceeds its respective strength.
  Maximum strain theory – similar, but based on strain limits.
  Tsai–Hill and Tsai–Wu – energy-based interaction criteria accounting for combined stresses.
  Hoffman and Hashin–Rotem – separate fibre and matrix failure modes.
  Puck criterion – distinguishes between fibre failure and inter-fibre (matrix-dominated) failure, offering high accuracy.
  Yamada–Sun and LaRC03 – advanced criteria that incorporate non-linear shear and multi-axial stress effects.
For bi-directional (woven) CFRP/GFRP (2D):
  Chang–Chang – empirical model that captures tension, compression, and shear damage modes for woven fabrics.
  Puck – extended to woven composites through modified stress interaction terms.
  Examples: analytical and numerical validations in Puck (2023) and Damghani et al. (2021) papers.
For 3D stress states:
  2D criteria are extended to account for out-of-plane stresses and interlaminar failure.
  3D Puck and 3D Hashin–Yamada–Sun include delamination and transverse cracking effects.
Key Takeaway
Failure in brittle composites is governed by strength-based failure theories rather than yield criteria.
The Puck criterion is widely regarded as one of the most accurate models, capable of distinguishing between fibre and matrix failures under complex multi-axial loading.
Advanced models (LaRC03, 3D Puck) form the foundation of modern finite element implementations used in aerospace composite design and certification.

## Slide 16
Maximum Stress Failure Criterion

## Slide 17: Failure criteria- Composite-Unidirectional- Maximum stress failure criterion
The principal stresses (, and ) in each ply are compared with their corresponding strength values (or also known as allowables):
  tensile strength in the ply direction (direction 1).
  compressive strength in the ply direction (direction 1).
  tensile strength perpendicular to the ply direction (direction 2).
  compressive strength perpendicular to the ply direction (direction 2).
  shear strength in 12-plane direction (within the plane of the ply).
Notes: Intro “This slide introduces the Maximum Stress Failure Criterion for unidirectional composite laminates. It is one of the simplest and most widely used strength-based approaches for predicting when a ply will fail under combined loading.”
Concept
The maximum stress criterion assumes each ply fails when any of its principal stress components exceed the corresponding material strength.
Failure is predicted independently for each stress direction—no interaction between stresses is considered.
The criterion uses allowable stresses (measured experimentally) in fibre, transverse, and shear directions.
Details
The ply’s principal stresses are compared with corresponding strength values:
  : tensile strength along the fibre (direction 1).
  : compressive strength along the fibre (direction 1).
  : tensile strength transverse to fibre (direction 2).
  : compressive strength transverse to fibre (direction 2).
  : in-plane shear strength ( plane).
Failure conditions:
  depending on whether the stress is tensile or compressive.
  depending on whether the stress is tensile or compressive.
  .
A ply is considered failed when any one of these conditions is violated.
The approach is easy to implement but ignores stress coupling and interaction effects between fibre and matrix.
The diagrams show how stress is resolved along fibre (1-direction) and transverse (2-direction) axes for unidirectional and cross-ply laminates.
Key Takeaway
The Maximum Stress Criterion provides a quick, conservative check for ply failure by comparing applied stresses to allowable limits.
It is best suited for preliminary design or cases where one stress component dominates.
For more complex multiaxial stress states, advanced interaction criteria (e.g., Tsai–Hill, Tsai–Wu) offer more accurate failure predictions.
Intro “This slide introduces the Maximum Stress Failure Criterion for unidirectional composite laminates. It is one of the simplest and most widely used strength-based approaches for predicting when a ply will fail under combined loading.”
Concept
The maximum stress criterion assumes each ply fails when any of its principal stress components exceed the corresponding material strength.
Failure is predicted independently for each stress direction—no interaction between stresses is considered.
The criterion uses allowable stresses (measured experimentally) in fibre, transverse, and shear directions.
Details
The ply’s principal stresses (𝜎_𝑥ⓜ,𝜎_𝑦ⓜ,𝜏_𝑥𝑦 )are compared with corresponding strength values:
  𝑋^𝑡: tensile strength along the fibre (direction 1).
  𝑋^𝑐: compressive strength along the fibre (direction 1).
  𝑌^𝑡: tensile strength transverse to fibre (direction 2).
  𝑌^𝑐: compressive strength transverse to fibre (direction 2).
  𝑆: in-plane shear strength (1"–" 2 plane).
Failure conditions:
  𝜎_𝑥<𝑋^𝑡 " or " 𝑋^𝑐depending on whether the stress is tensile or compressive.
  𝜎_𝑦<𝑌^𝑡 " or " 𝑌^𝑐depending on whether the stress is tensile or compressive.
  ∣𝜏_𝑥𝑦∣<𝑆.
A ply is considered failed when any one of these conditions is violated.
The approach is easy to implement but ignores stress coupling and interaction effects between fibre and matrix.
The diagrams show how stress is resolved along fibre (1-direction) and transverse (2-direction) axes for unidirectional and cross-ply laminates.
Key Takeaway
The Maximum Stress Criterion provides a quick, conservative check for ply failure by comparing applied stresses to allowable limits.
It is best suited for preliminary design or cases where one stress component dominates.
For more complex multiaxial stress states, advanced interaction criteria (e.g., Tsai–Hill, Tsai–Wu) offer more accurate failure predictions.

## Slide 18: Failure criteria- Composite-Unidirectional- Maximum stress failure criterion-Orders of magnitude of stresses at a fracture
  In cases where the ultimate elongation of the matrix is higher than that of the fibres, the longitudinal tensile strength of a unidirectional composite can be obtained by using the law of mixture:
  In practice it is quite difficult to obtain accurate values of .
  Example:
  E-glass fibres have a fracture stress of about 3,500 MPa. This decreases due to mechanical handling and chemical attacks before incorporation into the matrix. During the moulding process, their tensile strength is estimated to be between 1,500 and 2,500 MPa.
Notes: Intro “This slide explains how to estimate the longitudinal tensile strength of a unidirectional composite using the law of mixtures. It highlights how fibre strength, matrix contribution, and fibre volume fraction together determine the composite’s tensile capability.”
Concept
When the matrix elongation at failure is higher than that of the fibres, the fibre strength dominates the composite’s overall tensile strength.
The law of mixtures provides a first-order estimate:
where:
  : longitudinal tensile strength of the composite,
  : ultimate fibre strength,
  : fibre volume fraction,
  : stress in the matrix at the fibre’s ultimate strain.
Since the fibre contribution is dominant, this simplifies to:
Details
Practical limitations:
  Measuring accurately is difficult because fibres are fragile and can suffer surface damage, chemical degradation, or handling flaws before embedding.
  Fibre strength measured in isolation tends to be higher than when fibres are incorporated into a matrix.
Example:
  E-glass fibres have a nominal fracture strength of about 3,500 MPa, but this drops to 1,500–2,500 MPa once embedded, due to processing damage and imperfect fibre–matrix bonding.
  The figure shows the linear increase of with fibre volume fraction , bounded by these reduced strength values.
  In practical composites, typical ranges between 0.4 and 0.7, giving realistic tensile strengths around 900–1,500 MPa.
Key Takeaway
The longitudinal tensile strength of unidirectional composites primarily depends on the fibre strength and volume fraction.
While the law of mixtures gives a good approximation, real-world values are always lower due to processing defects, fibre damage, and non-ideal bonding.
Accurate experimental characterisation remains essential for reliable strength prediction and certification of composite structures.
Intro “This slide explains how to estimate the longitudinal tensile strength of a unidirectional composite using the law of mixtures. It highlights how fibre strength, matrix contribution, and fibre volume fraction together determine the composite’s tensile capability.”
Concept
When the matrix elongation at failure is higher than that of the fibres, the fibre strength dominates the composite’s overall tensile strength.
The law of mixtures provides a first-order estimate:
𝑋_𝑡=𝜎_𝑓𝑢 𝑉_𝑓+(𝜎_𝑚 ├ )┤_(𝜀_𝑓𝑢 ) (1−𝑉_𝑓 )┤
where:
  𝑋_𝑡: longitudinal tensile strength of the composite,
  𝜎_𝑓𝑢: ultimate fibre strength,
  𝑉_𝑓: fibre volume fraction,
  (𝜎_𝑚 ├ )┤_(𝜀_𝑓𝑢 ) ┤: stress in the matrix at the fibre’s ultimate strain.
Since the fibre contribution is dominant, this simplifies to:
𝑋_𝑡≈𝜎_𝑓𝑢 𝑉_𝑓
Details
Practical limitations:
  Measuring 𝜎_𝑓𝑢accurately is difficult because fibres are fragile and can suffer surface damage, chemical degradation, or handling flaws before embedding.
  Fibre strength measured in isolation tends to be higher than when fibres are incorporated into a matrix.
Example:
  E-glass fibres have a nominal fracture strength of about 3,500 MPa, but this drops to 1,500–2,500 MPa once embedded, due to processing damage and imperfect fibre–matrix bonding.
  The figure shows the linear increase of 𝑋_𝑡with fibre volume fraction 𝑉_𝑓, bounded by these reduced strength values.
  In practical composites, typical 𝑉_𝑓ranges between 0.4 and 0.7, giving realistic tensile strengths around 900–1,500 MPa.
Key Takeaway
The longitudinal tensile strength of unidirectional composites primarily depends on the fibre strength and volume fraction.
While the law of mixtures gives a good approximation, real-world values are always lower due to processing defects, fibre damage, and non-ideal bonding.
Accurate experimental characterisation remains essential for reliable strength prediction and certification of composite structures.

## Slide 19: Failure criteria- Composite-Unidirectional- Maximum stress failure criterion-Orders of magnitude of stresses at a fracture
  Typical strength values measured for various epoxide matrix composites:
  is constant with the fibre fraction and generally .
  is higher than and generally .
  is not dependant on the proportion of the fibres and is of the same order of magnitude of shear stress of the resin.
Notes: Intro “This slide presents typical strength values for unidirectional and balanced-cloth epoxy composites. These data illustrate how fibre type and volume fraction affect tensile, compressive, and shear strengths along and across the fibres.”
Concept
Each composite’s strength depends on the fibre material, orientation, and volume fraction (Vf).
The table compares unidirectional composites (E-glass, carbon, Kevlar) and a balanced carbon cloth laminate.
The main strength parameters are:
  : longitudinal tensile and compressive strengths.
  : transverse tensile and compressive strengths.
  : in-plane shear strength.
Details
Typical values (for epoxy matrix composites):
  : 0.4-0.6 most unidirectional systems.
  : 1300-1400 MPa for unidirectional composites; ~500 MPa for balanced woven carbon fabric.
  : ranges from 280 MPa (Kevlar) to 1,430 MPa (carbon).
  : typically, 15–50 MPa for unidirectional laminates; up to 460 MPa for woven carbon due to multi-directional reinforcement.
  : 100-350 MPa consistently higher than .
  : 35-70 MPa relatively constant across materials since it is dominated by the matrix shear strength.
Observed relationships:
  remains nearly independent of fibre content—controlled mainly by matrix tensile properties.
  is significantly higher than , typically , reflecting matrix confinement.
  depends on resin shear strength rather than fibre type or content, generally 35–70 MPa for epoxies.
Key Takeaway
Longitudinal strengths () are fibre-dominated, while transverse and shear strengths () are matrix-controlled.
Transverse compression () consistently exceeds transverse tension (), and shear strength remains relatively constant across composite systems.
These typical values serve as practical benchmarks for validating analytical models and material test data in composite design and certification.
Intro “This slide presents typical strength values for unidirectional and balanced-cloth epoxy composites. These data illustrate how fibre type and volume fraction affect tensile, compressive, and shear strengths along and across the fibres.”
Concept
Each composite’s strength depends on the fibre material, orientation, and volume fraction (Vf).
The table compares unidirectional composites (E-glass, carbon, Kevlar) and a balanced carbon cloth laminate.
The main strength parameters are:
  𝑋_𝑡,𝑋_𝑐: longitudinal tensile and compressive strengths.
  𝑌_𝑡,𝑌_𝑐: transverse tensile and compressive strengths.
  𝑆: in-plane shear strength.
Details
Typical values (for epoxy matrix composites):
  𝑉_𝑓: 0.4–0.6 for most unidirectional systems.
  𝑋_𝑡: 1,300–1,400 MPa for unidirectional composites; ~500 MPa for balanced woven carbon fabric.
  𝑋_𝑐: ranges from 280 MPa (Kevlar) to 1,430 MPa (carbon).
  𝑌_𝑡: typically 15–50 MPa for unidirectional laminates; up to 460 MPa for woven carbon due to multi-directional reinforcement.
  𝑌_𝑐: 100–350 MPa, consistently higher than 𝑌_𝑡.
  𝑆: ~35–70 MPa, relatively constant across materials since it is dominated by the matrix shear strength.
Observed relationships:
  𝑌_𝑡remains nearly independent of fibre content—controlled mainly by matrix tensile properties.
  𝑌_𝑐is significantly higher than 𝑌_𝑡, typically 100≤𝑌_𝑐≤150" MPa", reflecting matrix confinement.
  𝑆depends on resin shear strength rather than fibre type or content, generally 35–70 MPa for epoxies.
Key Takeaway
Longitudinal strengths (𝑋_𝑡,𝑋_𝑐) are fibre-dominated, while transverse and shear strengths (𝑌_𝑡,𝑌_𝑐,𝑆) are matrix-controlled.
Transverse compression (𝑌_𝑐) consistently exceeds transverse tension (𝑌_𝑡), and shear strength remains relatively constant across composite systems.
These typical values serve as practical benchmarks for validating analytical models and material test data in composite design and certification.

## Slide 20: Failure criteria- Composite-Unidirectional- Maximum stress failure criterion-Off-axis Tension or Compression
In tensile test:
In compressive test:
Smallest value of stress is chosen as strength
Maximum stress criteria for uni- glass fibre composite
A rapid logarithmic decline of strength
Notes: Intro “This slide explains how the Maximum Stress Failure Criterion applies to off-axis loading in unidirectional composites. It shows how tensile and compressive strength change sharply with fibre orientation relative to the loading direction.”
Concept
When a unidirectional composite is loaded at an angle (θ) to the fibre direction, the applied stress is resolved into:
  Longitudinal stress (σL) along the fibres,
  Transverse stress (σT) across the fibres,
  In-plane shear stress (σLT) between them.
These stresses are expressed as:
Failure occurs when any of these exceeds their respective strengths (Xt, Xc, Yt, Yc, S).
The smallest limiting value among these defines the composite’s effective strength in that off-axis direction.
Details
In tensile loading:
In compressive loading:
As the fibre orientation deviates from 0°, the load-carrying capacity drops steeply because the applied stress is no longer aligned with the fibres.
The graph shows a rapid logarithmic decline in strength as θ increases from 0° to ~15°, then levels off toward the matrix-dominated regime beyond 45°.
At large angles, the material’s strength is governed primarily by matrix tension, compression, or shear rather than fibre properties.
Key Takeaway
Off-axis strength decreases rapidly with increasing fibre misalignment due to reduced fibre contribution and higher shear stresses.
The maximum stress criterion effectively captures this trend, making it a useful first approximation for predicting anisotropic behaviour in composites.
In real design, fibre angles near the principal load direction should be maintained below ~15° to avoid significant loss of tensile or compressive strength.
Intro “This slide explains how the Maximum Stress Failure Criterion applies to off-axis loading in unidirectional composites. It shows how tensile and compressive strength change sharply with fibre orientation relative to the loading direction.”
Concept
When a unidirectional composite is loaded at an angle (θ) to the fibre direction, the applied stress is resolved into:
  Longitudinal stress (σL) along the fibres,
  Transverse stress (σT) across the fibres,
  In-plane shear stress (σLT) between them.
These stresses are expressed as:
𝜎_𝐿=𝜎_𝑥𝑥 〖cos⁡ 〗^2 𝜃, 𝜎_𝑇=𝜎_𝑥𝑥 〖sin⁡ 〗^2 𝜃, 𝜎_𝐿𝑇=−𝜎_𝑥𝑥 sin⁡𝜃 cos⁡𝜃
Failure occurs when any of these exceeds their respective strengths (Xt, Xc, Yt, Yc, S).
The smallest limiting value among these defines the composite’s effective strength in that off-axis direction.
Details
In tensile loading:
𝜎_𝑥𝑢=min⁡(𝑋_𝑡/(〖cos⁡ 〗^2 𝜃)ⓜ,𝑌_𝑡/(〖sin⁡ 〗^2 𝜃)ⓜ,𝑆/(sin⁡𝜃 cos⁡𝜃 ))
In compressive loading:
𝜎_𝑥𝑢=min⁡((∣𝑋_𝑐∣)/(〖cos⁡ 〗^2 𝜃)ⓜ,(∣𝑌_𝑐∣)/(〖sin⁡ 〗^2 𝜃)ⓜ,𝑆/(sin⁡𝜃 cos⁡𝜃 ))
As the fibre orientation deviates from 0°, the load-carrying capacity drops steeply because the applied stress is no longer aligned with the fibres.
The graph shows a rapid logarithmic decline in strength as θ increases from 0° to ~15°, then levels off toward the matrix-dominated regime beyond 45°.
At large angles, the material’s strength is governed primarily by matrix tension, compression, or shear rather than fibre properties.
Key Takeaway
Off-axis strength decreases rapidly with increasing fibre misalignment due to reduced fibre contribution and higher shear stresses.
The maximum stress criterion effectively captures this trend, making it a useful first approximation for predicting anisotropic behaviour in composites.
In real design, fibre angles near the principal load direction should be maintained below ~15° to avoid significant loss of tensile or compressive strength.

## Slide 21
Maximum Strain Failure Criterion

## Slide 22: Failure criteria- Composite-Unidirectional- Maximum strain failure criterion
The principal strains (, and ) in each ply are compared with their corresponding strain allowables:
  tensile strain allowable in the ply direction (direction 1).
  compressive strain allowable in the ply direction (direction 1).
  tensile strain allowable perpendicular to the ply direction (direction 2).
  compressive strain allowable perpendicular to the ply direction (direction 2).
  shear strain allowable in 12-plane direction (within the plane of the ply).
Notes: Intro “This slide presents the Maximum Strain Failure Criterion for unidirectional composites. It is similar in philosophy to the Maximum Stress Criterion but evaluates failure based on strain limits rather than stress values.”
Concept
Each ply fails when any of its principal strains exceed the corresponding strain allowable.
The method compares the measured or calculated strains in each ply to their allowable values:
  : allowable longitudinal tensile and compressive strains (direction 1).
  : allowable transverse tensile and compressive strains (direction 2).
  : allowable in-plane shear strain.
Failure occurs when any one component exceeds its corresponding allowable, ignoring interaction effects.
Details
For longitudinal direction (1-axis):
  or , depending on whether loading is tensile or compressive.
For transverse direction (2-axis):
  or .
For in-plane shear:
  .
This method is practical because strain data are directly measurable using strain gauges or digital image correlation (DIC).
The diagrams show unidirectional and cross-ply laminates with local ply coordinate systems, reinforcing that strain limits must be applied in each ply’s material axes.
The approach is often used in FEA post-processing, where ply-level strain outputs are compared to experimental allowables to identify first-ply failure.
Key Takeaway
The Maximum Strain Criterion is easy to apply and directly linked to experimental strain data.
It provides a conservative estimate of failure, especially useful when stress interactions are uncertain.
However, it ignores coupling between tension, compression, and shear, so for complex load cases, interaction-based models (Tsai–Hill, Tsai–Wu, or Puck) are preferred.
Intro “This slide presents the Maximum Strain Failure Criterion for unidirectional composites. It is similar in philosophy to the Maximum Stress Criterion but evaluates failure based on strain limits rather than stress values.”
Concept
Each ply fails when any of its principal strains exceed the corresponding strain allowable.
The method compares the measured or calculated strains (𝜀_𝑥ⓜ,𝜀_𝑦ⓜ,𝛾_𝑥𝑦 )in each ply to their allowable values:
  𝜀_𝑥𝑢^𝑡,𝜀_𝑥𝑢^𝑐: allowable longitudinal tensile and compressive strains (direction 1).
  𝜀_𝑦𝑢^𝑡,𝜀_𝑦𝑢^𝑐: allowable transverse tensile and compressive strains (direction 2).
  𝛾_𝑥𝑦𝑢: allowable in-plane shear strain.
Failure occurs when any one component exceeds its corresponding allowable, ignoring interaction effects.
Details
For longitudinal direction (1-axis):
  𝜀_𝑥<𝜀_𝑥𝑢^𝑡or 𝜀_𝑥<𝜀_𝑥𝑢^𝑐, depending on whether loading is tensile or compressive.
For transverse direction (2-axis):
  𝜀_𝑦<𝜀_𝑦𝑢^𝑡or 𝜀_𝑦<𝜀_𝑦𝑢^𝑐.
For in-plane shear:
  ∣𝛾_𝑥𝑦∣<𝛾_𝑥𝑦𝑢.
This method is practical because strain data are directly measurable using strain gauges or digital image correlation (DIC).
The diagrams show unidirectional and cross-ply laminates with local ply coordinate systems, reinforcing that strain limits must be applied in each ply’s material axes.
The approach is often used in FEA post-processing, where ply-level strain outputs are compared to experimental allowables to identify first-ply failure.
Key Takeaway
The Maximum Strain Criterion is easy to apply and directly linked to experimental strain data.
It provides a conservative estimate of failure, especially useful when stress interactions are uncertain.
However, it ignores coupling between tension, compression, and shear, so for complex load cases, interaction-based models (Tsai–Hill, Tsai–Wu, or Puck) are preferred.

## Slide 23: Failure criteria- Composite-Unidirectional- Maximum strain failure criterion-Off-axis Tension or Compression
In tensile test:
In compressive test:
Smallest value of stress is chosen as strength
Notes: Intro “This slide extends the Maximum Strain Failure Criterion to off-axis tension and compression in unidirectional composites. It explains how strain transformation equations are used to predict failure when the applied load is not aligned with the fibre direction.”
Concept
When a unidirectional laminate is loaded at an angle , the applied strain components are transformed from the global coordinate system to the local ply coordinates (L, T).
The Maximum Strain Criterion checks whether the principal strains in the ply exceed their corresponding tensile or compressive allowables.
The critical stress causing failure depends on both fibre orientation and material anisotropy.
Details
Transformed strain relations:
Failure conditions:
  Tensile or compressive limits are reached when any transformed strain exceeds the allowable:
Determination of off-axis strength:
  For tension:
  For compression:
The smallest calculated value corresponds to the off-axis strength of the ply.
As fibre angle increases, fibre contribution decreases and failure transitions from fibre-dominated (low θ) to matrix-dominated (high θ) behaviour.
Key Takeaway
The Maximum Strain Criterion for off-axis loading captures how fibre orientation affects tensile and compressive response.
Strength drops steeply with increasing angle due to lower stiffness and greater shear interaction.
This method provides a first-order but insightful prediction of directional dependence in composite failure, supporting more advanced multi-axial criteria like Tsai–Wu or Puck.
Intro “This slide extends the Maximum Strain Failure Criterion to off-axis tension and compression in unidirectional composites. It explains how strain transformation equations are used to predict failure when the applied load is not aligned with the fibre direction.”
Concept
When a unidirectional laminate is loaded at an angle 𝜃, the applied strain components are transformed from the global coordinate system to the local ply coordinates (L, T).
The Maximum Strain Criterion checks whether the principal strains in the ply exceed their corresponding tensile or compressive allowables.
The critical stress causing failure depends on both fibre orientation and material anisotropy.
Details
Transformed strain relations:
𝜀_𝐿=1/𝐸_𝐿 (〖cos⁡ 〗^2 𝜃−𝜈_𝐿𝑇 〖sin⁡ 〗^2 𝜃) 𝜎_𝑥𝑥
𝜀_𝑇=1/𝐸_𝑇 (〖sin⁡ 〗^2 𝜃−𝜈_𝑇𝐿 〖cos⁡ 〗^2 𝜃) 𝜎_𝑥𝑥
𝛾_𝐿𝑇=1/𝐺_𝐿𝑇 sin⁡𝜃 cos⁡𝜃 𝜎_𝑥𝑥
Failure conditions:
  Tensile or compressive limits are reached when any transformed strain exceeds the allowable:
−𝑋_𝑐<𝜎_𝑥𝑥 〖cos⁡ 〗^2 𝜃<𝑋_𝑡
−𝑌_𝑐<𝜎_𝑥𝑥 〖sin⁡ 〗^2 𝜃<𝑌_𝑡
−𝑆<−𝜎_𝑥𝑥 sin⁡𝜃 cos⁡𝜃<𝑆
Determination of off-axis strength:
  For tension:
𝜎_𝑥𝑢=min⁡(𝑋_𝑡/(〖cos⁡ 〗^2 𝜃−𝜈_𝐿𝑇 〖sin⁡ 〗^2 𝜃)ⓜ,𝑌_𝑡/(〖sin⁡ 〗^2 𝜃−𝜈_𝐿𝑇 〖cos⁡ 〗^2 𝜃)ⓜ,𝑆/(sin⁡𝜃 cos⁡𝜃 ))
  For compression:
𝜎_𝑥𝑢=min⁡((∣𝑋_𝑐∣)/(〖cos⁡ 〗^2 𝜃−𝜈_𝐿𝑇 〖sin⁡ 〗^2 𝜃)ⓜ,(∣𝑌_𝑐∣)/(〖sin⁡ 〗^2 𝜃−𝜈_𝐿𝑇 〖cos⁡ 〗^2 𝜃)ⓜ,𝑆/(sin⁡𝜃 cos⁡𝜃 ))
The smallest calculated value corresponds to the off-axis strength of the ply.
As fibre angle increases, fibre contribution decreases and failure transitions from fibre-dominated (low θ) to matrix-dominated (high θ) behaviour.
Key Takeaway
The Maximum Strain Criterion for off-axis loading captures how fibre orientation affects tensile and compressive response.
Strength drops steeply with increasing angle due to lower stiffness and greater shear interaction.
This method provides a first-order but insightful prediction of directional dependence in composite failure, supporting more advanced multi-axial criteria like Tsai–Wu or Puck.

## Slide 24
Tsai-Hill Failure Criterion

## Slide 25: Failure criteria- Composite-Unidirectional- Tsai-Hill failure criterion
Good for preliminary design due to simplicity.
Considers the interaction of stresses (based on experiments).
Does not distinguish between tensile or compressive forces.
It smears properties of plies, i.e. treating plies as homogeneous orthotropic material.
Failure types such as matrix cracking and fibre failure are not considered.
For a single ply under plane stress, we have:
Notes: Intro “This slide introduces the Tsai–Hill failure criterion, one of the earliest and simplest interaction-based theories used for composite laminates. It extends the von Mises yield concept to orthotropic materials such as unidirectional CFRP or GFRP plies.”
Concept
The Tsai–Hill criterion predicts failure when the combined effect of normal and shear stresses exceeds a critical limit.
It is based on the distortion energy theory, adapted to anisotropic (direction-dependent) materials.
The criterion assumes the composite behaves as a homogeneous orthotropic layer, smearing out fibre and matrix behaviour.
It is independent of the sign of the stresses, meaning it cannot distinguish between tension and compression failures.
Details
For a single ply under plane stress, the failure condition is given by:
where:
  : longitudinal strength (fibre direction),
  : transverse strength (matrix direction),
  : in-plane shear strength.
The terms are empirical coefficients often written as:
Advantages:
  Simple to apply and widely implemented in FEA software.
  Accounts for interaction between σx, σy, and τxy, unlike the Maximum Stress or Strain criteria.
  Suitable for preliminary design and laminate-level optimisation.
Limitations:
  Cannot differentiate between tension and compression failures.
  Does not predict fibre vs. matrix failure modes.
  Not suitable for post-failure progression or damage-tolerant analysis.
Key Takeaway
The Tsai–Hill criterion is an effective, easy-to-use tool for quick failure screening in composite laminates.
It provides reasonable accuracy for early design stages but should be replaced by more advanced criteria (Tsai–Wu, Hashin, or Puck) when mode-specific or directional failure mechanisms must be captured.
-----------------------------------------------------------------------------------------------------------------------------------------------------------------------------
Critical Note:
Intro
The distortion energy method, also called the von Mises criterion in metals, predicts material failure by focusing on the energy that changes shape rather than the energy that merely changes volume. This concept provides the foundation for several composite failure models, including the Tsai–Hill criterion.
Concept
Total strain energy in a material under load can be split into two parts:
  Volumetric energy — from uniform expansion or compression.
  Distortion energy — from shape change or shear deformation.
Ductile materials (like metals) fail when the distortion energy reaches a critical value equal to that at yielding in a simple tension test.
For anisotropic materials like composites, this same philosophy is extended: failure is assumed to occur when the combined distortion effects from all normal and shear stresses reach a critical value related to the material’s directional strengths.
Details
The von Mises criterion (for isotropic metals) is expressed as
where is the yield stress.
The Tsai–Hill criterion adapts this concept to orthotropic composite plies, combining fibre-directional stresses and shear:
where:
  = tensile strengths along fibre and transverse directions,
  = in-plane shear strength,
  = stresses in ply coordinates.
The criterion assumes that failure is governed by total distortion energy, not by any single stress component. Tension, compression, and shear all contribute to the same “shape-changing energy bucket.”
In composites, this gives a smooth, continuous failure surface rather than abrupt “box-like” limits seen in maximum stress or strain theories.
Key Takeaway
The distortion energy method connects metallic and composite failure logic. It says: a structure fails when its internal shape-changing energy matches that at failure in a simpler uniaxial test. In composites, Tsai–Hill generalises this principle to anisotropic materials—summing the effects of tension, compression, and shear into one energy-based criterion that captures how real laminates fail under complex loads.
Intro “This slide introduces the Tsai–Hill failure criterion, one of the earliest and simplest interaction-based theories used for composite laminates. It extends the von Mises yield concept to orthotropic materials such as unidirectional CFRP or GFRP plies.”
Concept
The Tsai–Hill criterion predicts failure when the combined effect of normal and shear stresses exceeds a critical limit.
It is based on the distortion energy theory, adapted to anisotropic (direction-dependent) materials.
The criterion assumes the composite behaves as a homogeneous orthotropic layer, smearing out fibre and matrix behaviour.
It is independent of the sign of the stresses, meaning it cannot distinguish between tension and compression failures.
Details
For a single ply under plane stress, the failure condition is given by:
(𝜎_𝑥/𝑋)^2−(𝜎_𝑥 𝜎_𝑦)/𝑋^2 +(𝜎_𝑦/𝑌)^2+(𝜏_𝑥𝑦/𝑆)^2=1
where:
  𝑋: longitudinal strength (fibre direction),
  𝑌: transverse strength (matrix direction),
  𝑆: in-plane shear strength.
The terms 𝐹_𝑥,𝐹_𝑦,𝐹_𝑥𝑦,𝐹_𝑠are empirical coefficients often written as:
𝐹_𝑥=1/𝑋^2 , 𝐹_𝑦=1/𝑌^2 , 𝐹_𝑠=1/𝑆^2
Advantages:
  Simple to apply and widely implemented in FEA software.
  Accounts for interaction between σx, σy, and τxy, unlike the Maximum Stress or Strain criteria.
  Suitable for preliminary design and laminate-level optimisation.
Limitations:
  Cannot differentiate between tension and compression failures.
  Does not predict fibre vs. matrix failure modes.
  Not suitable for post-failure progression or damage-tolerant analysis.
Key Takeaway
The Tsai–Hill criterion is an effective, easy-to-use tool for quick failure screening in composite laminates.
It provides reasonable accuracy for early design stages but should be replaced by more advanced criteria (Tsai–Wu, Hashin, or Puck) when mode-specific or directional failure mechanisms must be captured.

## Slide 26
Hoffman Failure Criterion

## Slide 27: Failure criteria- Composite-Unidirectional- Hoffman failure criterion
A generalised Hill’s criterion (experimental) that takes account of differences between the behaviours of material under tension and compressions was formulated by Hoffman.
Material fails if the following is met:
In the case of plane stress state (in plane of L, T and T’ or 1, 2 and 3, respectively)
=1
=2
=3
Tsai-Hill
Notes: Intro “This slide introduces the Hoffman failure criterion, an extension of Hill’s theory that accounts for the different tensile and compressive strengths of composite materials. It improves on Tsai–Hill by incorporating material asymmetry under tension and compression.”
Concept
The Hoffman criterion is an experimental generalisation of Hill’s theory, designed to model the anisotropic and non-symmetric strength behaviour of fibre composites.
It recognises that composites are stronger in tension than in compression (or vice versa), particularly along the fibre and transverse directions.
This makes Hoffman more realistic than Tsai–Hill for predicting failure under combined tension–compression states.
Details
Failure occurs when the following condition is satisfied:
The coefficients to are defined using the material strengths in each principal direction (L = fibre, T = transverse, T′ = through-thickness):
Under plane stress conditions (σ3 = 0), the full 3D equation simplifies to:
This form retains the stress interaction terms like Tsai–Hill but adds linear terms in σL and σT to represent the tension–compression asymmetry.
The figure illustrates how principal stresses (σL, σT, σLT) vary with fibre orientation and how the Hoffman surface differs from the symmetric Tsai–Hill ellipse.
Key Takeaway
The Hoffman criterion improves upon Tsai–Hill by distinguishing between tensile and compressive strengths, making it more accurate for non-symmetric composite behaviour.
It remains computationally simple and suitable for FEA applications and preliminary failure prediction.
However, it still cannot distinguish between fibre-dominated and matrix-dominated failure modes, requiring more advanced criteria (e.g., Hashin, Puck) for progressive damage analysis.
## Lecture: The Hoffman Failure Criterion 🧪
When a composite material is subjected to a complex combination of stresses (tension, compression, and shear all at once), how do we predict when it will fail? We can't just compare one stress to one strength. Instead, we use a failure criterion—a mathematical equation that combines all the stresses into a single condition for failure.
Today, we'll look at the Hoffman failure criterion, a powerful tool for this purpose.
## Background: The Tsai-Hill Criterion
Before Hoffman, a common model was the Tsai-Hill criterion. It's a good starting point but has one major limitation.
Tsai-Hill Equation:
The Problem: This equation uses single strength values ( for longitudinal, for transverse). It assumes the material is equally strong in tension and compression, which is rarely true for composites. For example, a carbon fibre composite is much stronger in longitudinal tension than in longitudinal compression.
## The Hoffman Criterion: A More Realistic Model ✅
The Hoffman criterion is a generalized, experimental model that improves upon Tsai-Hill by addressing its key weakness.
Key Advantage: It explicitly accounts for the different strengths of the material under tension and compression.
The Hoffman Equation (for 2D Plane Stress):
This equation looks complex, but it's just combining the applied stresses (σL​,σT​,τLT​) with the material's known strengths.
## How to Use the Criterion 💥
To use the Hoffman criterion, you need five fundamental material strength properties:
: Longitudinal Tensile Strength (along the fibres)
: Longitudinal Compressive Strength
: Transverse Tensile Strength (perpendicular to fibres)
: Transverse Compressive Strength
: In-Plane Shear Strength
The process is simple:
Determine the stresses acting on the material in its principal directions ().
Plug these stresses and the five material strengths into the left-hand side of the Hoffman equation. This value is called the Failure Index (FI).
Check the result:
  If FI < 1, the material is considered safe.
  If FI ≥ 1, the material is predicted to have failed.
## Key Takeaway
The Hoffman criterion is a robust method for predicting composite failure under combined loading. Its primary advantage is its ability to differentiate between tensile and compressive strengths, leading to more accurate and realistic failure predictions than simpler models.
Intro “This slide introduces the Hoffman failure criterion, an extension of Hill’s theory that accounts for the different tensile and compressive strengths of composite materials. It improves on Tsai–Hill by incorporating material asymmetry under tension and compression.”
Concept
The Hoffman criterion is an experimental generalisation of Hill’s theory, designed to model the anisotropic and non-symmetric strength behaviour of fibre composites.
It recognises that composites are stronger in tension than in compression (or vice versa), particularly along the fibre and transverse directions.
This makes Hoffman more realistic than Tsai–Hill for predicting failure under combined tension–compression states.
Details
Failure occurs when the following condition is satisfied:
𝐶_1 (𝜎_𝑇−𝜎_(𝑇^′ ) ├ )┤^2+𝐶_2 (𝜎_(𝑇^′ )−𝜎_𝐿 ├ )┤^2+𝐶_3 (𝜎_𝐿−𝜎_𝑇 ├ )┤^2+𝐶_4 𝜎_𝐿+𝐶_5 𝜎_𝑇+𝐶_6 𝜎_(𝑇^′ )+𝐶_7 𝜎_(𝑇^′)^2+𝐶_8 𝜎_𝐿𝑇^2+𝐶_9 𝜎_(𝐿𝑇^′)^2=1┤┤┤
The coefficients 𝐶_1to 𝐶_9are defined using the material strengths in each principal direction (L = fibre, T = transverse, T′ = through-thickness):
𝐶_1=1/2 (1/(𝑌_𝑡 𝑌_𝑐 )+1/(𝑍_𝑡 𝑍_𝑐 )−1/(𝑋_𝑡 𝑋_𝑐 )), 𝐶_4=1/𝑋_𝑡 −1/𝑋_𝑐 , 𝐶_7=1/(𝑆_(𝑇𝑇^′)^2 )," etc."
Under plane stress conditions (σ3 = 0), the full 3D equation simplifies to:
(𝜎_𝐿^2)/(𝑋_𝑡 𝑋_𝑐 )+(𝜎_𝑇^2)/(𝑌_𝑡 𝑌_𝑐 )−(𝜎_𝐿 𝜎_𝑇)/(𝑋_𝑡 𝑋_𝑐 )+(𝑋_𝑐−𝑋_𝑡)/(𝑋_𝑡 𝑋_𝑐 ) 𝜎_𝐿+(𝑌_𝑐−𝑌_𝑡)/(𝑌_𝑡 𝑌_𝑐 ) 𝜎_𝑇+(𝜏_𝐿𝑇^2)/(𝑆_𝐿𝑇^2 )=1
This form retains the stress interaction terms like Tsai–Hill but adds linear terms in σL and σT to represent the tension–compression asymmetry.
The figure illustrates how principal stresses (σL, σT, σLT) vary with fibre orientation and how the Hoffman surface differs from the symmetric Tsai–Hill ellipse.
Key Takeaway
The Hoffman criterion improves upon Tsai–Hill by distinguishing between tensile and compressive strengths, making it more accurate for non-symmetric composite behaviour.
It remains computationally simple and suitable for FEA applications and preliminary failure prediction.
However, it still cannot distinguish between fibre-dominated and matrix-dominated failure modes, requiring more advanced criteria (e.g., Hashin, Puck) for progressive damage analysis.
## Lecture: The Hoffman Failure Criterion 🧪
When a composite material is subjected to a complex combination of stresses (tension, compression, and shear all at once), how do we predict when it will fail? We can't just compare one stress to one strength. Instead, we use a failure criterion—a mathematical equation that combines all the stresses into a single condition for failure.
Today, we'll look at the Hoffman failure criterion, a powerful tool for this purpose.
## Background: The Tsai-Hill Criterion
Before Hoffman, a common model was the Tsai-Hill criterion. It's a good starting point but has one major limitation.
Tsai-Hill Equation:
The Problem: This equation uses single strength values ( for longitudinal, for transverse). It assumes the material is equally strong in tension and compression, which is rarely true for composites. For example, a carbon fibre composite is much stronger in longitudinal tension than in longitudinal compression.
## The Hoffman Criterion: A More Realistic Model ✅
The Hoffman criterion is a generalized, experimental model that improves upon Tsai-Hill by addressing its key weakness.
Key Advantage: It explicitly accounts for the different strengths of the material under tension and compression.
The Hoffman Equation (for 2D Plane Stress):
This equation looks complex, but it's just combining the applied stresses (σL​,σT​,τLT​) with the material's known strengths.
## How to Use the Criterion 💥
To use the Hoffman criterion, you need five fundamental material strength properties:
: Longitudinal Tensile Strength (along the fibres)
: Longitudinal Compressive Strength
: Transverse Tensile Strength (perpendicular to fibres)
: Transverse Compressive Strength
: In-Plane Shear Strength
The process is simple:
Determine the stresses acting on the material in its principal directions ().
Plug these stresses and the five material strengths into the left-hand side of the Hoffman equation. This value is called the Failure Index (FI).
Check the result:
  If FI < 1, the material is considered safe.
  If FI ≥ 1, the material is predicted to have failed.
## Key Takeaway
The Hoffman criterion is a robust method for predicting composite failure under combined loading. Its primary advantage is its ability to differentiate between tensile and compressive strengths, leading to more accurate and realistic failure predictions than simpler models.

## Slide 28
Tsai-Wu Failure Criterion

## Slide 29: Failure criteria- Composite-Unidirectional- Tsai-Wu failure criterion
This criterion results from an attempt to mathematically generalise the Tsai-Hill criterion.
It acknowledges the fact that composites have different strength in tension and compression.
Good for preliminary design due to simplicity.
It includes a curve fitting aspect and is not purely experimental.
It smears properties of plies, i.e. treating plies as homogeneous orthotropic material.
Failure types such as matrix cracking and fibre failure are not considered.
For a single ply under plane stress, we have:
Tsai-Wu provides unrealistic values for biaxial loading. For other loading types, it gives values that are either acceptable or excellent compared to the experimental results.
Tsai-Hill
Notes: Intro “This slide expands on the Tsai–Wu failure criterion, one of the most widely used theories for predicting the onset of failure in anisotropic composites such as CFRP and GFRP. It provides a unified quadratic formulation that considers both tensile–compressive asymmetry and stress interactions.”
Concept
The Tsai–Wu criterion was developed to extend Tsai–Hill by incorporating different strengths in tension and compression for anisotropic materials.
It defines a quadratic failure surface that predicts failure when the combined stresses exceed a material-dependent limit.
The model captures interaction effects between normal and shear stresses and can represent multi-axial stress states in laminates.
Failure is assumed to occur when the stress state reaches the boundary of a failure envelope in stress space.
Details
The general Tsai–Wu equation under plane stress is:
Key features:
  Includes tensile and compressive strength asymmetry through linear terms.
  Quadratic terms define the interaction between stress components.
  Defines a failure envelope: stresses inside are safe; stresses outside cause failure.
Failure modes considered implicitly:
  Longitudinal and transverse tension/compression (σx, σy).
  In-plane shear (τxy).
Although it does not explicitly separate fibre, matrix, or delamination failure, it provides an overall laminate failure prediction.
Advantages
Comprehensive interaction: captures coupling between normal and shear stresses.
Tension–compression distinction: includes separate strengths for tension and compression.
Versatile application: suitable for both unidirectional and woven CFRP/GFRP laminates.
Broad FEA compatibility: implemented in software such as ANSYS, Abaqus, and NASTRAN for composite failure prediction.
Good for preliminary and laminate-level design: gives conservative and realistic predictions for most loading types.
Limitations
No explicit fibre–matrix mode separation: cannot distinguish matrix cracking from fibre breakage.
No progressive damage modelling: only predicts first-ply failure, not subsequent load redistribution.
Material constants required: needs accurate tension and compression strengths in all directions.
No delamination prediction: interlaminar effects are outside its scope.
Biaxial loading sensitivity: may produce unrealistic results under certain combined compressive stress states.
Key Takeaway
The Tsai–Wu criterion is a robust, general-purpose failure model for composites that effectively handles multi-directional stress interactions.
It provides reliable predictions for first-ply failure in both unidirectional and woven laminates, especially under complex loading.
For complete failure analysis, Tsai–Wu is often combined with progressive damage models or mode-specific criteria such as Hashin or Puck to capture fibre breakage, matrix cracking, and delamination more precisely.
ChatGPT can make mista
Intro “This slide expands on the Tsai–Wu failure criterion, one of the most widely used theories for predicting the onset of failure in anisotropic composites such as CFRP and GFRP. It provides a unified quadratic formulation that considers both tensile–compressive asymmetry and stress interactions.”
Concept
The Tsai–Wu criterion was developed to extend Tsai–Hill by incorporating different strengths in tension and compression for anisotropic materials.
It defines a quadratic failure surface that predicts failure when the combined stresses exceed a material-dependent limit.
The model captures interaction effects between normal and shear stresses and can represent multi-axial stress states in laminates.
Failure is assumed to occur when the stress state reaches the boundary of a failure envelope in stress space.
Details
The general Tsai–Wu equation under plane stress is:
(𝜎_𝑥^2)/(𝑋_𝑡 𝑋_𝑐 )+(𝜎_𝑦^2)/(𝑌_𝑡 𝑌_𝑐 )−√(1/(𝑋_𝑡 𝑋_𝑐 𝑌_𝑡 𝑌_𝑐 )) " " 𝜎_𝑥 𝜎_𝑦+(1/𝑋_𝑡 −1/𝑋_𝑐 ) 𝜎_𝑥+(1/𝑌_𝑡 −1/𝑌_𝑐 ) 𝜎_𝑦+(𝜏_𝑥𝑦^2)/𝑆^2 =1
Key features:
  Includes tensile and compressive strength asymmetry through linear terms.
  Quadratic terms define the interaction between stress components.
  Defines a failure envelope: stresses inside are safe; stresses outside cause failure.
Failure modes considered implicitly:
  Longitudinal and transverse tension/compression (σx, σy).
  In-plane shear (τxy).
Although it does not explicitly separate fibre, matrix, or delamination failure, it provides an overall laminate failure prediction.
Advantages
Comprehensive interaction: captures coupling between normal and shear stresses.
Tension–compression distinction: includes separate strengths for tension and compression.
Versatile application: suitable for both unidirectional and woven CFRP/GFRP laminates.
Broad FEA compatibility: implemented in software such as ANSYS, Abaqus, and NASTRAN for composite failure prediction.
Good for preliminary and laminate-level design: gives conservative and realistic predictions for most loading types.
Limitations
No explicit fibre–matrix mode separation: cannot distinguish matrix cracking from fibre breakage.
No progressive damage modelling: only predicts first-ply failure, not subsequent load redistribution.
Material constants required: needs accurate tension and compression strengths in all directions.
No delamination prediction: interlaminar effects are outside its scope.
Biaxial loading sensitivity: may produce unrealistic results under certain combined compressive stress states.
Key Takeaway
The Tsai–Wu criterion is a robust, general-purpose failure model for composites that effectively handles multi-directional stress interactions.
It provides reliable predictions for first-ply failure in both unidirectional and woven laminates, especially under complex loading.
For complete failure analysis, Tsai–Wu is often combined with progressive damage models or mode-specific criteria such as Hashin or Puck to capture fibre breakage, matrix cracking, and delamination more precisely.
ChatGPT can make mista

## Slide 30: Keynote
The Hoffman and Tsai–Wu criteria are closely related.
Tsai–Wu is essentially a mathematical generalisation of Hoffman.
Both evolved from the Hill and von Mises distortion energy concept, but they differ in how they treat tension–compression asymmetry and interaction terms.
Hoffman = Experimental Hill: practical, data-driven, reliable for composites under known loading states.
Tsai–Wu = Generalised Energy Polynomial: elegant and adaptable but needs careful calibration and may overpredict failure under biaxial or triaxial stress.

## Slide 31
LARC03 Failure Criterion

## Slide 32: Failure criteria- Composite-Unidirectional- LARC03
Notes: Intro “This slide presents the LARC03 (Laminated Analysis of Realistic Composites, version 03) failure model — a NASA-developed progressive damage criterion for fibre-reinforced composites. Unlike simpler static failure theories, LARC03 predicts both damage initiation and subsequent degradation of material properties under complex loading.”
Concept
LARC03 was developed to improve on earlier criteria such as Hashin and Chang–Chang, addressing their inability to model progressive damage and the transition between fibre- and matrix-dominated failures.
It provides separate equations for each major failure mode — fibre tension, fibre compression, matrix tension, and matrix compression — while accounting for interlaminar shear and fibre-misalignment effects.
The model is designed for laminated CFRP/GFRP structures in aerospace and high-performance engineering, where accurate life prediction under multiaxial loading is critical.
Details
Failure Modes Defined in LARC03:
  Fibre Tension (FT): Occurs when longitudinal stress σ₁₁ ≥ 0 exceeds the fibre tensile strength Xᵗ. Leads to fibre breakage or splitting.
  Fibre Compression (FC): Initiated when σ₁₁ ≤ 0 and fibres buckle or kink; depends on shear coupling between matrix and fibre.
  Matrix Tension (MT): Driven by tensile stress σ₂₂ ≥ 0 in the transverse direction, resulting in matrix cracking, debonding, or fibre–matrix separation.
  Matrix Compression (MC): Triggered when σ₂₂ ≤ 0, causing crushing, shear failure, or micro-buckling in the matrix.
Mathematical Framework (examples shown in figure):
  The model defines matrix cracking functions (Fᴹ) for tension and compression and fibre failure functions (Fᶠ) for tension and compression using strength allowables Yᵗ, Yᶜ, Xᵗ, Xᶜ and in-situ strengths Sᴸᵢₛ, Yᵢₛ.
  Failure initiation occurs when Fᴹ or Fᶠ ≥ 1.
  Optional parameters α₀ and ηᴸ describe ply thickness and misalignment effects.
  In-situ strengths Yᵢₛ and Sᴸᵢₛ are derived from fracture-mechanics-based scaling relations involving energy release rates Gᵢ꜀(L).
Progressive Damage Implementation:
  After initiation, stiffness and strength are reduced iteratively in the damaged elements (often by material degradation or element deactivation in FEA).
  This allows load redistribution and simulation of global failure progression.
  The model supports 2D and 3D applications in finite element codes for realistic composite structures.
Advantages:
  Handles multiple failure mechanisms with clear physical meaning.
  Models progressive stiffness and strength degradation, not just first-ply failure.
  Incorporates fibre-misalignment and thickness effects, improving predictive accuracy.
  Readily implemented in FEA tools (e.g. Abaqus, MSC Nastran, ANSYS).
Limitations:
  Requires extensive material characterisation (E₁, E₂, G₁₂, ν₁₂, Xᵗ, Xᶜ, Yᵗ, Yᶜ, Sᴸ, Gᵢ꜀).
  Computationally intensive compared with simpler static models.
  May need coupling with delamination criteria for full interlaminar failure prediction.
Key Takeaway
LARC03 is a high-fidelity, physics-based progressive damage model capable of predicting both initiation and growth of fibre and matrix failures in laminated composites.
It combines fracture-mechanics scaling with in-situ strength formulations to simulate realistic behaviour under multiaxial stress states.
The model has become a benchmark for aerospace-grade CFRP design, offering greater predictive power than static criteria like Tsai-Wu or Hashin, particularly in multi-ply, damage-tolerant analysis.

## Slide 33
Hashin-Rotem Failure Criterion

## Slide 34: Failure criteria- Composite-Unidirectional- Hashin-Rotem failure criterion
Fibre failure:
Matrix failure:
Notes: Intro “This slide presents the Hashin–Rotem failure criterion, a physically based approach for predicting distinct failure modes in fibre-reinforced composites such as CFRP and GFRP. Unlike earlier isotropic theories, Hashin–Rotem separates fibre- and matrix-dominated failures, providing a more realistic description of anisotropic composite behaviour under multi-axial loading.”
Concept
Developed by Zvi Hashin and Avraham Rotem, this criterion identifies four independent failure modes corresponding to the fibre and matrix under tension and compression.
The theory is based on the stress state in the local ply coordinate system (1–2 axes).
It assumes that failure occurs when the corresponding stress combination in fibre or matrix exceeds the respective strength limit.
The separation of fibre and matrix contributions allows the model to better represent the anisotropic nature of laminated composites.
Details
Fibre tension failure (FT):
  Occurs when σ₁ ≥ 0 and σ₁/Xᵗ ≥ 1.
  Represents fibre breakage or splitting along the fibre direction.
  Typical in high axial tension or load-aligned conditions.
Fibre compression failure (FC):
  Occurs when σ₁ ≤ 0 and |σ₁|/Xᶜ ≥ 1.
  Represents fibre buckling or kinking under compressive loads.
  Common in bending-dominated or impact-loaded laminates.
Matrix tension failure (MT):
  For σ₂ ≥ 0, failure occurs when
  Indicates cracking or fibre–matrix debonding due to transverse tensile stress.
Matrix compression failure (MC):
  For σ₂ ≤ 0, failure occurs when
  Represents matrix crushing, shearing, or local instability under transverse compression.
Key assumptions:
  The material is transversely isotropic in each ply.
  Each failure mode is independent and does not interact with others until progressive damage modelling is introduced.
  Strengths Xᵗ, Xᶜ, Yᵗ, Yᶜ, and S are determined experimentally.
Advantages
Distinguishes clearly between fibre- and matrix-dominated failure.
Handles tension and compression asymmetry, a key improvement over Tsai–Hill.
Computationally simple and easily implemented in analytical or finite element frameworks.
Provides good agreement with experimental results for unidirectional laminates.
Limitations
Does not include progressive damage or stiffness degradation.
Ignores interaction between failure modes (e.g. fibre–matrix coupling).
Not directly applicable to woven composites without modification.
Requires separate treatment for delamination or interlaminar shear failure.
Key Takeaway
The Hashin–Rotem criterion provides a physically intuitive and experimentally validated framework for identifying failure in composites, separating fibre tension/compression from matrix tension/compression.
It remains one of the foundational criteria for unidirectional CFRP/GFRP analysis and forms the conceptual basis for advanced progressive damage models such as Hashin (1980), Chang–Chang, and LARC03 used in aerospace structural design.
Intro “This slide presents the Hashin–Rotem failure criterion, a physically based approach for predicting distinct failure modes in fibre-reinforced composites such as CFRP and GFRP. Unlike earlier isotropic theories, Hashin–Rotem separates fibre- and matrix-dominated failures, providing a more realistic description of anisotropic composite behaviour under multi-axial loading.”
Concept
Developed by Zvi Hashin and Avraham Rotem, this criterion identifies four independent failure modes corresponding to the fibre and matrix under tension and compression.
The theory is based on the stress state in the local ply coordinate system (1–2 axes).
It assumes that failure occurs when the corresponding stress combination in fibre or matrix exceeds the respective strength limit.
The separation of fibre and matrix contributions allows the model to better represent the anisotropic nature of laminated composites.
Details
Fibre tension failure (FT):
  Occurs when σ₁ ≥ 0 and σ₁/Xᵗ ≥ 1.
  Represents fibre breakage or splitting along the fibre direction.
  Typical in high axial tension or load-aligned conditions.
Fibre compression failure (FC):
  Occurs when σ₁ ≤ 0 and |σ₁|/Xᶜ ≥ 1.
  Represents fibre buckling or kinking under compressive loads.
  Common in bending-dominated or impact-loaded laminates.
Matrix tension failure (MT):
  For σ₂ ≥ 0, failure occurs when
(𝜎_2/𝑌^𝑡 )^2+(𝜏_12/𝑆)^2=1
  Indicates cracking or fibre–matrix debonding due to transverse tensile stress.
Matrix compression failure (MC):
  For σ₂ ≤ 0, failure occurs when
(𝜎_2/𝑌^𝑐 )^2+(𝜏_12/𝑆)^2=1
  Represents matrix crushing, shearing, or local instability under transverse compression.
Key assumptions:
  The material is transversely isotropic in each ply.
  Each failure mode is independent and does not interact with others until progressive damage modelling is introduced.
  Strengths Xᵗ, Xᶜ, Yᵗ, Yᶜ, and S are determined experimentally.
Advantages
Distinguishes clearly between fibre- and matrix-dominated failure.
Handles tension and compression asymmetry, a key improvement over Tsai–Hill.
Computationally simple and easily implemented in analytical or finite element frameworks.
Provides good agreement with experimental results for unidirectional laminates.
Limitations
Does not include progressive damage or stiffness degradation.
Ignores interaction between failure modes (e.g. fibre–matrix coupling).
Not directly applicable to woven composites without modification.
Requires separate treatment for delamination or interlaminar shear failure.
Key Takeaway
The Hashin–Rotem criterion provides a physically intuitive and experimentally validated framework for identifying failure in composites, separating fibre tension/compression from matrix tension/compression.
It remains one of the foundational criteria for unidirectional CFRP/GFRP analysis and forms the conceptual basis for advanced progressive damage models such as Hashin (1980), Chang–Chang, and LARC03 used in aerospace structural design.
ChatGPT ca

## Slide 35: Example
Consider an orthotropic layer whose characteristics at fracture are given by:
This layer is subjected to a tension in the direction .
Plot (first in Cartesian coordinates for , then in polar coordinates for ), the tensile strength as a function of the angle of tension, using the maximum stress criterion.
Notes: Intro “This slide sets up a worked example: given ply strengths and an off-axis tensile load at angle θ, compute and plot the tensile strength σxu versus θ using the Maximum Stress Criterion.”
Concept
Use the Maximum Stress Criterion under tensile loading.
Resolve the applied stress at angle θ into local ply components and compare each with its allowable.
For tension, governing limits are Xt, Yt, and S only.
Details
Given allowables: , , , , .
Transform a uniaxial tensile stress applied at angle θ to local ply stresses:
Off-axis tensile strength is the smallest value that trips any limit:
Check anchor points to guide the plot:
  (fibre-dominated).
  (shear-dominated).
  (matrix-dominated).
Expected curve shape: sharp drop from 1500 MPa near , passing through a valley controlled by S near ≈ 160 MPa, then approaching Yt = 90 MPa as .
For a Cartesian plot: graph versus .
For a polar plot: plot radius for using symmetry (repeat every ).
Key Takeaway
Off-axis tensile strength collapses rapidly with misalignment: fibre-dominated near , shear-limited around , and matrix-limited near .
With the given allowables, the laminate falls from 1500 MPa at to about 160 MPa near and 90 MPa at ; design should keep primary load paths within ~ of the fibres to avoid this steep strength loss.
Intro “This slide sets up a worked example: given ply strengths and an off-axis tensile load at angle θ, compute and plot the tensile strength σxu versus θ using the Maximum Stress Criterion.”
Concept
Use the Maximum Stress Criterion under tensile loading.
Resolve the applied stress at angle θ into local ply components and compare each with its allowable.
For tension, governing limits are Xt, Yt, and S only.
Details
Given allowables: 𝑋_𝑡=1500" MPa", 𝑋_𝑐=1700" MPa", 𝑌_𝑡=90" MPa", 𝑌_𝑐=250" MPa", 𝑆=80" MPa".
Transform a uniaxial tensile stress 𝜎_𝑥𝑥applied at angle θ to local ply stresses:
  𝜎_𝐿=𝜎_𝑥𝑥 〖cos⁡ 〗^2 𝜃
  𝜎_𝑇=𝜎_𝑥𝑥 〖sin⁡ 〗^2 𝜃
  𝜏_𝐿𝑇=−𝜎_𝑥𝑥 sin⁡𝜃 cos⁡𝜃
Off-axis tensile strength is the smallest value that trips any limit:
𝜎_𝑥𝑢 (𝜃)=min⁡" ⁣" ( 𝑋_𝑡/(〖cos⁡ 〗^2 𝜃)ⓜ," " ⓜ,𝑌_𝑡/(〖sin⁡ 〗^2 𝜃) " " 𝑆/(sin⁡𝜃 cos⁡𝜃 )), 0≤𝜃≤90^∘
Check anchor points to guide the plot:
  𝜃=0^∘:" " 𝜎_𝑥𝑢=𝑋_𝑡=1500" MPa"(fibre-dominated).
  (shear-dominated).
  𝜃=90^∘:" " 𝜎_𝑥𝑢=𝑌_𝑡=90" MPa"(matrix-dominated).
Expected curve shape: sharp drop from 1500 MPa near 0^∘, passing through a valley controlled by S near 45^∘≈ 160 MPa, then approaching Yt = 90 MPa as 𝜃→90^∘.
For a Cartesian plot: graph 𝜎_𝑥𝑢versus 𝜃∈[0ⓜ,90^∘ ].
For a polar plot: plot radius =𝜎_𝑥𝑢 (𝜃)for 𝜃∈[0ⓜ,360^∘ ]using symmetry (repeat every 90^∘).
Key Takeaway
Off-axis tensile strength collapses rapidly with misalignment: fibre-dominated near 0^∘, shear-limited around 45^∘, and matrix-limited near 90^∘.
With the given allowables, the laminate falls from 1500 MPa at 0^∘to about 160 MPa near 45^∘and 90 MPa at 90^∘; design should keep primary load paths within ~15^∘ of the fibres to avoid this steep strength loss.

## Slide 36: Solution
See file “Maximum Stress Criterion Example-1.xls” for detailed solution.
Illustration in the cartesian graph is shown below:
Chart: Angle (deg)
| 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90
 | 1500 | 467.8087 | 248.9158 | 184.7521 | 162.4683 | 153.3679 | 120 | 101.9227 | 92.7982 | 90
Notes: Intro “This slide shows the numerical and graphical solution of the previous example, illustrating how tensile strength of an orthotropic layer varies with fibre angle under the Maximum Stress Criterion.”
Concept
The Maximum Stress Criterion assumes failure when any principal stress exceeds its corresponding allowable in tension, compression, or shear.
By resolving applied stress at angle θ, we can evaluate which mode governs failure—fibre, matrix, or shear.
The resulting strength variation with θ represents the directional dependence of composite strength, or its anisotropy.
Details
Material allowables used: .
The off-axis tensile strength is evaluated using:
for .
Graph interpretation:
  At θ = 0°, load aligns with fibres → fibre tension failure dominates at 1500 MPa.
  Between 10° and 45°, shear stresses become critical → strength drops sharply to ~160 MPa.
  At θ ≈ 90°, matrix tensile failure governs → ~90 MPa.
The curve shows the nonlinear drop in tensile strength as fibres rotate away from load direction, confirming strong anisotropy.
Such trends are typical of unidirectional CFRP or GFRP laminates and demonstrate that fibre alignment is crucial to maintaining strength.
Key Takeaway
The Maximum Stress Criterion provides a simple but effective way to visualise the drastic strength reduction caused by fibre misalignment.
The chart highlights three regions:
  Fibre-dominated (0°–10°): high load capacity.
  Shear-dominated (~30°–50°): steep strength loss.
  Matrix-dominated (>70°): lowest strength.
Design implication: for high-strength applications, loads should remain within ±15° of the fibre axis to avoid shear-driven failure.
Intro “This slide shows the numerical and graphical solution of the previous example, illustrating how tensile strength of an orthotropic layer varies with fibre angle under the Maximum Stress Criterion.”
Concept
The Maximum Stress Criterion assumes failure when any principal stress exceeds its corresponding allowable in tension, compression, or shear.
By resolving applied stress at angle θ, we can evaluate which mode governs failure—fibre, matrix, or shear.
The resulting strength variation with θ represents the directional dependence of composite strength, or its anisotropy.
Details
Material allowables used: 𝑋_𝑡=1500" MPa"," " 𝑋_𝑐=1700" MPa"," " 𝑌_𝑡=90" MPa"," " 𝑌_𝑐=250" MPa"," " 𝑆=80" MPa".
The off-axis tensile strength is evaluated using:
𝜎_𝑥𝑢 (𝜃)=min⁡" ⁣" ( 𝑋_𝑡/(〖cos⁡ 〗^2 𝜃)ⓜ," " ⓜ,𝑌_𝑡/(〖sin⁡ 〗^2 𝜃) " " 𝑆/(sin⁡𝜃 cos⁡𝜃 ))
for 0°≤𝜃≤90°.
Graph interpretation:
  At θ = 0°, load aligns with fibres → fibre tension failure dominates at 1500 MPa.
  Between 10° and 45°, shear stresses become critical → strength drops sharply to ~160 MPa.
  At θ ≈ 90°, matrix tensile failure governs → ~90 MPa.
The curve shows the nonlinear drop in tensile strength as fibres rotate away from load direction, confirming strong anisotropy.
Such trends are typical of unidirectional CFRP or GFRP laminates and demonstrate that fibre alignment is crucial to maintaining strength.
Key Takeaway
The Maximum Stress Criterion provides a simple but effective way to visualise the drastic strength reduction caused by fibre misalignment.
The chart highlights three regions:
  Fibre-dominated (0°–10°): high load capacity.
  Shear-dominated (~30°–50°): steep strength loss.
  Matrix-dominated (>70°): lowest strength.
Design implication: for high-strength applications, loads should remain within ±15° of the fibre axis to avoid shear-driven failure.

## Slide 37: Solution
Chart: 
| 0 | 20 | 40 | 60 | 80 | 100 | 120 | 140 | 160 | 180 | 200 | 220 | 240 | 260 | 280 | 300 | 320 | 340
 | 1500 | 248.9158 | 162.4683 | 120 | 92.7982 | 92.7982 | 120 | 162.4683 | 248.9158 | 1500 | 248.9158 | 162.4683 | 120 | 92.7982 | 92.7982 | 120 | 162.4683 | 248.9158
The polar graph is shown here:
Notes: Intro “This polar plot visualises the same off-axis tensile strength variation (σxu vs θ) obtained from the Maximum Stress Criterion, now displayed as a radial representation to illustrate anisotropy.”
Concept
In a polar plot, the radius corresponds to the tensile strength , and the angle represents fibre orientation relative to the loading direction.
The plot is symmetric every 90°, reflecting orthotropic symmetry in the composite lamina.
Details
Material allowables: .
At and : fibre-aligned → strength .
At and : shear-dominated → strength .
At and : matrix-dominated → strength .
The elongated vertical axis represents the high longitudinal strength along fibres, while the narrow lateral spread indicates weakness in the transverse and shear directions.
This creates the characteristic “peanut” shape typical of unidirectional composites, where strength is highest along fibres and minimal perpendicular to them.
Key Takeaway
The polar plot vividly demonstrates the directional dependency of composite strength.
Unidirectional laminates show extreme anisotropy: strong along fibres, weak transversely.
The plot reinforces the design rule that primary loads should align with fibre direction to exploit full material capacity, while off-axis loading must be minimised or supported by cross-ply reinforcement.
Intro “This polar plot visualises the same off-axis tensile strength variation (σxu vs θ) obtained from the Maximum Stress Criterion, now displayed as a radial representation to illustrate anisotropy.”
Concept
In a polar plot, the radius corresponds to the tensile strength 𝜎_𝑥𝑢, and the angle 𝜃represents fibre orientation relative to the loading direction.
The plot is symmetric every 90°, reflecting orthotropic symmetry in the composite lamina.
Details
Material allowables: 𝑋_𝑡=1500" MPa"," " 𝑌_𝑡=90" MPa"," " 𝑆=80" MPa".
At 𝜃=0°and 180°: fibre-aligned → strength ≈1500" MPa".
At 𝜃=45°and 225°: shear-dominated → strength ≈160" MPa".
At 𝜃=90°and 270°: matrix-dominated → strength ≈90" MPa".
The elongated vertical axis represents the high longitudinal strength along fibres, while the narrow lateral spread indicates weakness in the transverse and shear directions.
This creates the characteristic “peanut” shape typical of unidirectional composites, where strength is highest along fibres and minimal perpendicular to them.
Key Takeaway
The polar plot vividly demonstrates the directional dependency of composite strength.
Unidirectional laminates show extreme anisotropy: strong along fibres, weak transversely.
The plot reinforces the design rule that primary loads should align with fibre direction to exploit full material capacity, while off-axis loading must be minimised or supported by cross-ply reinforcement.

## Slide 38: Failure criteria- Composite-Woven fabrics
There are nearly 20 failure theories derived for UD composite materials, while there is a very limited explicit failure criterion specifically developed and standardised for woven composites.
For woven bi-directional composites:
  The change in cross section of woven yarns over their longitudinal axes.
  Fibers are not straight in woven yarns like fibres in UD tows.
  Yarns can have in-plane waviness (misalignment) and out-of-plane waviness (crimping) in woven laminates, which considerably affect their tensile and bending behaviours.
  Interaction between the warp and weft yarns may affect the effective mechanical behaviours of woven laminates, especially under multidirectional/combined loading modes.
  Owing to a cellular reinforcement architecture, failure modes such as matrix cracking is restricted between weave cells in woven composites and cannot propagate as fast as it would in UDs.
  The interlacement of yarns can cause local stress concentrations at meso-level.
Weave cells
Notes: Intro “This slide introduces failure criteria for woven fabric composites, highlighting how their complex geometry—interlaced yarns, crimps, and weave architecture—fundamentally changes their failure behaviour compared to unidirectional (UD) composites.”
Concept
Most existing composite failure models (Tsai–Hill, Hashin, Puck, LARC03, etc.) were developed for unidirectional laminates, where fibres are straight and continuous.
Woven fabrics introduce additional mesoscale effects—yarn crimp, interlacing, and local curvature—which alter stress transfer and failure initiation.
These factors require modified or distinct failure models, yet no universal standard has been agreed upon due to the complexity of the woven architecture.
Details
Geometry and waviness effects:
  Each woven yarn experiences periodic cross-sectional variation and crimping, creating alternating zones of tension and compression along its path.
  Unlike UD composites, fibres in woven yarns are not straight, leading to local misalignment and early matrix micro-cracking under tension.
  In-plane waviness (yarn misalignment) and out-of-plane crimping (undulation between warp and weft) reduce stiffness and strength, particularly under combined loading.
Weave interaction:
  The warp–weft interaction produces nonlinear stress–strain response and influences failure mode transition under biaxial or shear loading.
  Local bending and shear at yarn crossovers induce stress concentrations, especially near interlacement points (weave cells).
Damage mechanisms:
  Tow misalignment leads to local shear-induced failure in the matrix between yarns.
  Ply wrinkling and binder misalignment in multi-ply woven laminates cause matrix cracking and delamination initiation.
  Due to the cellular reinforcement architecture, matrix cracking is constrained within the weave cells—damage growth is more gradual than in UD composites.
Mechanical consequence:
  Woven laminates typically exhibit higher damage tolerance but lower stiffness and strength than equivalent UD layups.
  Their performance depends strongly on weave type, yarn volume fraction, and crimp angle.
Key Takeaway
Unlike UD laminates, woven composites display multi-scale failure behaviour governed by yarn architecture and crimp.
Their interlaced geometry introduces local stress concentrations and anisotropic stiffness reduction, which complicate direct application of UD failure theories.
The lack of a standardised woven-fabric failure criterion remains an active research area—modern approaches combine mesoscale FEA, micromechanics, and digital image correlation (DIC) to characterise and validate realistic woven damage evolution.

## Slide 39: Failure criteria- Composite-Woven fabrics-Matrix cracking
Weave cells
F
F
Notes: Intro “This slide illustrates matrix cracking in woven fabric composites, focusing on how the unique weave architecture — with its interlaced yarns and resin-rich zones — localises and controls damage within individual weave cells.”
Concept
In woven composites, the resin matrix lies between crossing yarns (warp and weft).
When the laminate is loaded in tension or shear, the matrix between these yarns experiences high triaxial stresses.
The local stress concentration in resin pockets or at yarn–matrix interfaces initiates matrix microcracking, which often remains confined within each weave cell rather than propagating globally.
Details
Stress localisation:
  Under applied load (F), the periodic geometry of warp and weft creates alternating zones of tension and compression.
  Matrix regions between yarns act as weak links, where tensile and shear stresses combine to initiate cracks.
  The rectangular yellow schematic represents a unit weave cell, showing principal tension along one axis and compressive–shear response along the other.
Crack initiation and orientation:
  Cracks often begin near the yarn crossover regions, where resin-rich pockets form.
  These cracks are typically inclined, as shown in the deformed yellow cell, due to combined tensile and shear loading.
  Out-of-plane crimping and local yarn undulation further amplify local strain fields, promoting diagonal crack paths.
Matrix confinement:
  The crimped weave pattern causes cracks to arrest within a single cell rather than spreading across plies.
  This explains why woven laminates show higher damage tolerance compared to UD laminates — energy is dissipated locally through small, controlled cracks rather than catastrophic propagation.
Experimental observation:
  Microscopy and DIC studies show matrix cracks forming along the shear plane between interlaced tows, correlating with regions of high inter-yarn shear strain.
Key Takeaway
Matrix cracking in woven composites is a localised, geometry-driven failure mode confined by the weave architecture.
The interlacement of yarns enhances damage containment and toughness, but at the cost of reduced stiffness and early onset of microcracking.
Understanding this mechanism is essential for predicting failure initiation, especially in shear-dominated or biaxial loading of woven laminates.

## Slide 40
Chang-Chang Failure Criterion

## Slide 41: Failure criteria- Composite-Woven fabrics- Chang-chang
Chang-chang
The value of parameter defined interaction between shear and tensile stresses and is obtained experimentally.
In the terminology used in this lecture, recall that:
Notes: Intro
The Chang–Chang failure criterion is an experimentally derived model used to predict different failure modes in composite materials, particularly carbon-fibre reinforced polymers (CFRP). It was developed to capture the behaviour of both fibre and matrix failures under tension and compression, and is especially relevant for woven composites, where fibre crimping and interlacing modify the stress response.
Concept
Chang–Chang separates composite failure into four distinct modes:
  Fibre Tension Failure (FT): fibre rupture under longitudinal tensile load.
  Fibre Compression Failure (FC): fibre kinking or buckling under longitudinal compressive load.
  Matrix Tension Failure (MT): resin cracking or fibre–matrix debonding under transverse tensile load.
  Matrix Compression Failure (MC): matrix shear, crushing, or micro-buckling under transverse compressive load.
The model includes a coupling term (β) to account for interaction between shear and normal stresses.
Failure occurs when the mode-specific failure index ≥ 1.
Details
The failure indices are defined as:
Stress components correspond to in-plane laminate axes: .
The interaction coefficient β is obtained experimentally (typically between 0.3–1.0).
The model is suitable for FEA integration and is implemented in ABAQUS, ANSYS, and other composite solvers.
In woven CFRPs, fibre crimping, warp/weft interlacing, and matrix constraint between weave cells alter the local stress distribution. Chang–Chang remains valid provided homogenised ply properties are used.
Progressive failure can be modelled by degrading stiffness post-initiation.
Key Takeaway
Strength: Captures both fibre and matrix failures, with realistic shear–normal interaction.
Applicability: Effective for woven CFRPs under multiaxial stress states.
Limitation: Does not inherently predict delamination or progressive fibre–matrix decohesion—must be coupled with damage evolution models (e.g. cohesive zone).
Best Use: For preliminary and intermediate-level damage prediction in woven or multi-directional CFRP laminates.
Intro
The Chang–Chang failure criterion is an experimentally derived model used to predict different failure modes in composite materials, particularly carbon-fibre reinforced polymers (CFRP). It was developed to capture the behaviour of both fibre and matrix failures under tension and compression, and is especially relevant for woven composites, where fibre crimping and interlacing modify the stress response.
Concept
Chang–Chang separates composite failure into four distinct modes:
  Fibre Tension Failure (FT): fibre rupture under longitudinal tensile load.
  Fibre Compression Failure (FC): fibre kinking or buckling under longitudinal compressive load.
  Matrix Tension Failure (MT): resin cracking or fibre–matrix debonding under transverse tensile load.
  Matrix Compression Failure (MC): matrix shear, crushing, or micro-buckling under transverse compressive load.
The model includes a coupling term (β) to account for interaction between shear and normal stresses.
Failure occurs when the mode-specific failure index ≥ 1.
Details
The failure indices are defined as:
𝑒_𝑓^2=(𝜎_𝑎𝑎/𝑋_𝑡 )^2+𝛽(𝜎_𝑎𝑏/𝑆_𝑐 )^2−1≥0 ("fibre tension" )
𝑒_𝑐^2=(𝜎_𝑎𝑎/𝑋_𝑐 )^2−1≥0 ("fibre compression" )
𝑒_𝑚^2=(𝜎_𝑏𝑏/𝑌_𝑡 )^2+𝛽(𝜎_𝑎𝑏/𝑆_𝑐 )^2−1≥0 ("matrix tension" )
𝑒_𝑑^2=[𝑌_𝑐/(2𝑆_𝑐 )]^2−1+(𝜎_𝑎𝑏/𝑆_𝑐 )^2−1≥0 ("matrix compression" )
Stress components correspond to in-plane laminate axes: 𝜎_𝑎𝑎=𝜎_11," " 𝜎_𝑏𝑏=𝜎_22," " 𝜎_𝑎𝑏=𝜎_12.
The interaction coefficient β is obtained experimentally (typically between 0.3–1.0).
The model is suitable for FEA integration and is implemented in ABAQUS, ANSYS, and other composite solvers.
In woven CFRPs, fibre crimping, warp/weft interlacing, and matrix constraint between weave cells alter the local stress distribution. Chang–Chang remains valid provided homogenised ply properties are used.
Progressive failure can be modelled by degrading stiffness post-initiation.
Key Takeaway
Strength: Captures both fibre and matrix failures, with realistic shear–normal interaction.
Applicability: Effective for woven CFRPs under multiaxial stress states.
Limitation: Does not inherently predict delamination or progressive fibre–matrix decohesion—must be coupled with damage evolution models (e.g. cohesive zone).
Best Use: For preliminary and intermediate-level damage prediction in woven or multi-directional CFRP laminates.

## Slide 42
Puck Failure Criterion

## Slide 43: Failure criteria- Composite-Woven fabrics- Original Puck
Original Puck
  Puck-Schürmann modified the Hashin criteria, by considering the Fibre Failure (FF) basis to depend on the fibre physical properties (volume fractions etc) without involving the ply.
  The interlaminar stresses in the laminae were not taken into consideration by the Hashin or Puck and Schürmann criteria because they were both 2D criteria.
  Later versions of Puck criterion included interlaminar stresses.
  This new 3D Puck failure criteria is known as the action-plane failure criteria.
  The Puck criteria help identify the many lamina failure mechanisms and quantify the impact of each type of failure on the laminate.
Notes: READ “Puck’s Criterion for the tensile response of composite laminates: A numerical approach” by Anand Pai, Rishabh Suri, Aniket Kunal Bhave, Pranay Verma, Padmaraj N H published in Advances in Engineering Software 175 (2023) 103364.
Read: https://help.altair.com/hwdesktop/hwx/topics/panels/result_math_composites_operators_puck_criteria_r.htm
Intro
The Puck failure criterion, introduced by Puck and Schürmann, was developed to more accurately predict the distinct failure modes in fibre-reinforced composites. It modifies the Hashin criterion by explicitly separating fibre failure (FF) and inter-fibre failure (IFF) and linking fibre failure to the intrinsic fibre properties rather than the entire ply response.
Concept
Puck-Schürmann proposed that Fibre Failure (FF) should depend on fibre-level properties (e.g. fibre volume fraction, fibre strength, and stiffness) instead of laminate properties.
The matrix-dominated failures were described through inter-fibre failure (IFF) criteria that consider shear and normal stresses acting on potential fracture planes.
Early versions of the model were 2D, like Hashin, but later extensions introduced 3D formulations that include interlaminar stresses.
The 3D Puck criterion is now considered an action-plane failure theory, meaning that the stress state is projected onto a potential fracture plane to determine when and how failure initiates.
Details
The Puck criterion distinguishes three primary failure mechanisms:
  Fibre Failure (FF) in tension and compression
  Matrix Failure (IFF) under transverse tension, moderate compression, and large compression:
    Matrix tension:
    Moderate compression:
    Large compression:
Here, are fracture-plane dependent parameters, is the shear strength, and are transverse tensile and compressive strengths.
The inter-fibre failure (IFF) concept uniquely considers the local stress state around the fibre–matrix interface, where cracks typically initiate.
This physically based approach makes Puck’s theory superior for multi-directional laminates and woven composites, where matrix-dominated failures are critical.
Key Takeaway
Strength: Puck’s criterion captures fibre and matrix failure mechanisms separately, providing physical insight into initiation and propagation.
Advancement: Later 3D formulations include interlaminar stresses, extending predictive accuracy to thick or complex laminates.
Applicability: Highly suited for woven CFRP/GFRP where local bending, crimping, and inter-fibre shear dominate failure.
Limitation: Computationally intensive; requires calibration of multiple empirical parameters for each material system.
Best Use: For advanced FEA simulations and progressive damage analysis in aerospace-grade composites where detailed damage evolution is critical.
READ “Puck’s Criterion for the tensile response of composite laminates: A numerical approach” by Anand Pai, Rishabh Suri, Aniket Kunal Bhave, Pranay Verma, Padmaraj N H published in Advances in Engineering Software 175 (2023) 103364.
Read: https://help.altair.com/hwdesktop/hwx/topics/panels/result_math_composites_operators_puck_criteria_r.htm
Intro
The Puck failure criterion, introduced by Puck and Schürmann, was developed to more accurately predict the distinct failure modes in fibre-reinforced composites. It modifies the Hashin criterion by explicitly separating fibre failure (FF) and inter-fibre failure (IFF) and linking fibre failure to the intrinsic fibre properties rather than the entire ply response.
Concept
Puck-Schürmann proposed that Fibre Failure (FF) should depend on fibre-level properties (e.g. fibre volume fraction, fibre strength, and stiffness) instead of laminate properties.
The matrix-dominated failures were described through inter-fibre failure (IFF) criteria that consider shear and normal stresses acting on potential fracture planes.
Early versions of the model were 2D, similar to Hashin, but later extensions introduced 3D formulations that include interlaminar stresses.
The 3D Puck criterion is now considered an action-plane failure theory, meaning that the stress state is projected onto a potential fracture plane to determine when and how failure initiates.
Details
The Puck criterion distinguishes three primary failure mechanisms:
  Fibre Failure (FF) in tension and compression
1/𝜀_1𝑇 (𝜀_1+𝜈_12/𝐸_1 𝑚_𝑓 𝜎_22 )=1
1/𝜀_1𝐶 (𝜀_1+𝜈_12/𝐸_1 𝑚_𝑓 𝜎_22 )+(10𝜏_21 ├ )┤^2=1┤
  Matrix Failure (IFF) under transverse tension, moderate compression, and large compression:
    Matrix tension:
√((𝜏_21/𝑆_21 )^2+(1−𝑝_𝑣^+ 𝑌_𝑇/𝑆_21 )^2 (𝜎_22/𝑌_𝑇 )^2 )+𝑝_𝑣^+ 𝜎_22/𝑆_21 +𝜎_11/𝜎_11𝐷 =1
    Moderate compression:
1/𝑆_21 √((𝜏_21 ├ )┤^2+(𝑝_𝑣^− 𝜎_22 ├ )┤^2 ┤┤ )+𝜎_11/𝜎_11𝐷 =1
    Large compression:
[𝜏_21/(2(1+𝑝_𝑤^− ) 𝑆_21 )]^2+(𝜎_22/𝑌_𝐶 )^2+𝜎_11/𝜎_11𝐷 =1
Here, 𝑝_𝑣^+,𝑝_𝑣^−,𝑝_𝑤^−are fracture-plane dependent parameters, 𝑆_21is the shear strength, and 𝑌_𝑇,𝑌_𝐶are transverse tensile and compressive strengths.
The inter-fibre failure (IFF) concept uniquely considers the local stress state around the fibre–matrix interface, where cracks typically initiate.
This physically based approach makes Puck’s theory superior for multi-directional laminates and woven composites, where matrix-dominated failures are critical.
Key Takeaway
Strength: Puck’s criterion captures fibre and matrix failure mechanisms separately, providing physical insight into initiation and propagation.
Advancement: Later 3D formulations include interlaminar stresses, extending predictive accuracy to thick or complex laminates.
Applicability: Highly suited for woven CFRP/GFRP where local bending, crimping, and inter-fibre shear dominate failure.
Limitation: Computationally intensive; requires calibration of multiple empirical parameters for each material system.
Best Use: For advanced FEA simulations and progressive damage analysis in aerospace-grade composites where detailed damage evolution is critical.

## Slide 44: Failure criteria- Composite-Woven/unidirectional- Puck
2D Puck (as used by Altair)
Notes: READ “Puck’s Criterion for the tensile response of composite laminates: A numerical approach” by Anand Pai, Rishabh Suri, Aniket Kunal Bhave, Pranay Verma, Padmaraj N H published in Advances in Engineering Software 175 (2023) 103364.
Read: https://help.altair.com/hwdesktop/hwx/topics/panels/result_math_composites_operators_puck_criteria_r.htm
Failure Criteria – Composite (Woven / Unidirectional) – 2D Puck
Concept
The 2D Puck criterion is a simplification of the full 3D Puck–Schürmann theory, suitable for laminate-level FEA when only in-plane stresses are known.
It separates fibre failure (FF) and matrix or inter-fibre failure (IFF) and introduces empirical inclination parameters and to account for the effect of shear on transverse tensile / compressive failure.
Commercial solvers such as Altair OptiStruct, Abaqus, and Ansys ACP implement this 2D form for both UD and woven laminates.
Details
Fibre failure
Matrix failure is divided into three stress modes:
Mode A – Transverse Tension ()
Mode B – Moderate Compression ( and )
Mode C – Large Compression (otherwise)
Failure index
Failure occurs when .
Inclination parameters (empirical):
MaterialGFRP 0.25 0.30 CFRP 0.30 0.35 Others 0.20 0.30
These parameters modify the inclination of the fracture plane for tension (+) and compression (−), accounting for frictional shear coupling at the fibre–matrix interface.
Key Takeaway
Purpose: Provides a practical, computationally efficient version of the full Puck criterion for laminate FEA.
Strength: Captures matrix-shear coupling effects through ; accurate for woven and UD plies under combined tension–shear.
Limit: Neglects out-of-plane stresses (), so interlaminar and delamination failures require 3D Puck or cohesive models.
Industry Use: Implemented in Altair OptiStruct, Abaqus, and Ansys for progressive damage analysis of CFRP/GFRP laminates.
READ “Puck’s Criterion for the tensile response of composite laminates: A numerical approach” by Anand Pai, Rishabh Suri, Aniket Kunal Bhave, Pranay Verma, Padmaraj N H published in Advances in Engineering Software 175 (2023) 103364.
Read: https://help.altair.com/hwdesktop/hwx/topics/panels/result_math_composites_operators_puck_criteria_r.htm
Failure Criteria – Composite (Woven / Unidirectional) – 2D Puck
Concept
The 2D Puck criterion is a simplification of the full 3D Puck–Schürmann theory, suitable for laminate-level FEA when only in-plane stresses are known.
It separates fibre failure (FF) and matrix or inter-fibre failure (IFF) and introduces empirical inclination parameters 𝑃_∥^+and 𝑃_∥^−to account for the effect of shear on transverse tensile / compressive failure.
Commercial solvers such as Altair OptiStruct, Abaqus, and Ansys ACP implement this 2D form for both UD and woven laminates.
Details
Fibre failure
𝐹_"fiber" =∣𝜎_1/𝑋∣, 𝑋={■(𝑋_𝑇&"if " 𝜎_1≥0@𝑋_𝐶&"if " 𝜎_1<0)┤
Matrix failure is divided into three stress modes:
Mode A – Transverse Tension (𝜎_2>0)
𝐹_"matrix" ^𝐴=√((𝜏_12/𝑆)^2+(1−𝑃_∥^+ 𝑌_𝑇/𝑆)^2 (𝜎_2/𝑌_𝑇 )^2 )+𝑃_∥^+ 𝜎_2/𝑆
Mode B – Moderate Compression (𝜎_2<0 and 0<∣𝜎_2/𝜏_12∣<𝑅_𝐴1/∣𝜏_12𝑐∣)
𝐹_"matrix" ^𝐵=1/𝑆 √((𝜏_12 ├ )┤^2+(𝑃_∥^− 𝜎_2 ├ )┤^2 ┤┤ )+𝑃_∥^− 𝜎_2/𝑆
Mode C – Large Compression (otherwise)
𝐹_"matrix" ^𝐶=[𝜏_12/2(1+𝑃_∥^− )𝑆]^2+(𝜎_2/𝑌_𝐶 )^2
Failure index
Failure occurs when 𝐹_"index" ≥1.
Inclination parameters (empirical):
Material𝑃_∥^− 𝑃_∥^+GFRP0.250.30CFRP0.300.35Others0.200.30
These parameters modify the inclination of the fracture plane for tension (+) and compression (−), accounting for frictional shear coupling at the fibre–matrix interface.
Key Takeaway
Purpose: Provides a practical, computationally efficient version of the full Puck criterion for laminate FEA.
Strength: Captures matrix-shear coupling effects through 𝑃_∥^±; accurate for woven and UD plies under combined tension–shear.
Limit: Neglects out-of-plane stresses (𝜎_3,𝜏_13,𝜏_23), so interlaminar and delamination failures require 3D Puck or cohesive models.
Industry Use: Implemented in Altair OptiStruct, Abaqus, and Ansys for progressive damage analysis of CFRP/GFRP laminates.

## Slide 45
Yamada-Sun Failure Criterion

## Slide 46: Failure criteria- Composite-Woven fabrics- Yamada Sun
2D Yamada Sun
The equation indicates that failure occurs when the combination of transverse and shear stresses reaches the failure envelope defined by the material properties and .
This makes the Yamada-Sun criterion ideal for capturing matrix cracking, delamination, or failure where shear stress contributes significantly to matrix degradation.
Therefore, Yamada Sun is often used in combination with other failure criterion such as Hashin to capture fibre failure.
Notes: Intro
The Yamada–Sun criterion predicts matrix-dominated failure in fibre-reinforced composites, particularly under transverse tension and in-plane shear. It complements fibre-based criteria like Hashin or Tsai–Wu and is widely implemented in commercial FEA tools.
Concept
Developed by Yamada & Sun (1978) for predicting matrix cracking and delamination.
Based on interaction between transverse tensile (σ₂) and in-plane shear (τ₁₂) stresses.
Defines a failure envelope in the σ₂–τ₁₂ stress space.
Used alongside Hashin or Puck for a complete laminate failure description.
Details
Mathematical form:
where:
  = matrix tensile strength (transverse direction)
  = in-plane shear strength
Interpretation:
  If : matrix is safe.
  If : matrix failure initiates (cracking or delamination).
Failure mechanisms captured:
  Matrix tension failure: crack initiation perpendicular to fibres.
  Shear-driven delamination: ply separation due to τ₁₂–σ₂ coupling.
  Matrix compression failure: approximated by combining Yamada–Sun with Hashin modes.
In woven CFRP:
  Fibre crimp and resin-rich regions amplify τ₁₂, accelerating matrix cracking.
  Criterion valid for both warp and weft directions due to symmetric weave.
  Used in progressive damage simulations to predict onset of delamination.
Industrial relevance:
  Implemented in Altair OptiStruct, and Ansys ACP under 2D failure modes.
  Recommended for impact, bending, and interlaminar shear studies.
Key Takeaway
The Yamada–Sun model is essential for predicting matrix cracking and delamination in woven and unidirectional CFRPs.
It captures transverse–shear coupling, providing more realistic predictions than maximum stress or strain criteria.
However, it must be paired with fibre-based models (Hashin, Puck, Tsai–Wu) for a full laminate-level failure assessment.
Its simplicity and accuracy make it a preferred tool in aerospace composite FEA for early damage detection and certification analyses.
Intro
The Yamada–Sun criterion predicts matrix-dominated failure in fibre-reinforced composites, particularly under transverse tension and in-plane shear. It complements fibre-based criteria like Hashin or Tsai–Wu and is widely implemented in commercial FEA tools.
Concept
Developed by Yamada & Sun (1978) for predicting matrix cracking and delamination.
Based on interaction between transverse tensile (σ₂) and in-plane shear (τ₁₂) stresses.
Defines a failure envelope in the σ₂–τ₁₂ stress space.
Used alongside Hashin or Puck for a complete laminate failure description.
Details
Mathematical form:
𝐹_"index" =(𝜎_2/𝑌_𝑡 )^2+(𝜏_12/𝑆)^2=1
where:
  𝑌_𝑡= matrix tensile strength (transverse direction)
  𝑆= in-plane shear strength
Interpretation:
  If 𝐹_"index" <1: matrix is safe.
  If 𝐹_"index" ≥1: matrix failure initiates (cracking or delamination).
Failure mechanisms captured:
  Matrix tension failure: crack initiation perpendicular to fibres.
  Shear-driven delamination: ply separation due to τ₁₂–σ₂ coupling.
  Matrix compression failure: approximated by combining Yamada–Sun with Hashin modes.
In woven CFRP:
  Fibre crimp and resin-rich regions amplify τ₁₂, accelerating matrix cracking.
  Criterion valid for both warp and weft directions due to symmetric weave.
  Used in progressive damage simulations to predict onset of delamination.
Industrial relevance:
  Implemented in Altair OptiStruct, Abaqus, and Ansys ACP under 2D failure modes.
  Recommended for impact, bending, and interlaminar shear studies.
Key Takeaway
The Yamada–Sun model is essential for predicting matrix cracking and delamination in woven and unidirectional CFRPs.
It captures transverse–shear coupling, providing more realistic predictions than maximum stress or strain criteria.
However, it must be paired with fibre-based models (Hashin, Puck, Tsai–Wu) for a full laminate-level failure assessment.
Its simplicity and accuracy make it a preferred tool in aerospace composite FEA for early damage detection and certification analyses.

## Slide 47: Summary
Criterion Name | Best For | Pros | Cons | Notes
Max-Stress / Max-Strain | Early sizing and hand checks | Simple and intuitive | No interaction; conservative | Good first screen per ply
Hoffman / Tsai–Wu | General in-plane loading | Captures interaction; Hoffman models asymmetry | Less physically specific | Hoffman coefficients map directly to allowables
Hashin / Puck | High-fidelity ply physics in FEA | Identifies mode; robust correlation | More parameters; calibration | Puck is superior for matrix-dominated failures
Yamada–Sun / Chang–Chang | Woven and ±45° matrix-dominated onset | Captures σ₂–τ₁₂ interaction; fabric-friendly | Needs pairing for fibre modes | Use with a fibre criterion and a degradation law
LaRC03 | Certification-level progressive simulation | Predicts stiffness loss and residual strength | Computationally intensive | Separate FT, FC, MT, MC initiation and evolution

## Slide 48: Laminate failure
So far, we discussed various theories to express the failure of each composite ply.
A composite laminate is comprised of several plies.
The question is that, in design and analysis, when do we consider the laminate as failed?
  First ply failure
  Progressive failure
Ply 1
Ply 2
Ply k
.
.
.
Ply k-1
Notes: Intro In composite laminate analysis, understanding how and when a laminate is considered “failed” is critical. While ply-level criteria (Hashin, Puck, Tsai–Wu, etc.) predict failure initiation within individual layers, laminate failure involves assessing the global integrity of the entire stack.
Concept
A composite laminate consists of multiple plies, each with different fibre orientations and stress states.
Each ply may fail at different loads or strain levels, leading to progressive rather than instantaneous failure.
Designers must define a failure criterion at the laminate level — either at the first indication of local failure or when the structure can no longer sustain load.
Details
First Ply Failure (FPF):
  The laminate is considered failed when the first ply reaches its failure criterion (e.g., Hashin index ≥ 1).
  Conservative approach — often used in certification or preliminary design.
  Does not account for residual strength or load redistribution.
Progressive (Last Ply) Failure (LPF):
  The laminate continues to carry load after initial ply failures.
  Material properties of failed plies are degraded, and analysis continues until global collapse.
  More realistic for actual structures and often used in nonlinear FEA or damage-tolerant design.
Transition between the two:
  In aerospace design, FPF defines design allowables, while LPF (progressive failure) defines ultimate load capacity.
  Progressive models use stiffness degradation laws (e.g., Puck, LARC03, or continuum damage mechanics).
Key Takeaway
First Ply Failure (FPF) → Conservative, used for safe design limits.
Progressive Failure (LPF) → Realistic, used for damage tolerance and residual strength analysis.
The laminate is not necessarily “failed” when a ply fails — the true structural failure depends on the cumulative damage and residual load-bearing capacity.

## Slide 49: Laminate failure- First Ply Failure (FPF)
The opposite laminate is made of k number of plies.
Assume that the entire laminate fails after First Ply Failure (FPF).
Let’s assume Ply 1 fails first, then we assume the entire laminate has failed.
The approach is conservative.
Good for initial design phases where expensive computational power is not critical.
See animation (top right corner).
Ply 1
Ply 2
Ply k
.
.
.
Ply k-1
Ply 1
Ply 2
Ply k
Ply k-1
Notes: Intro First Ply Failure (FPF) represents the onset of laminate failure — the point when the first ply in a composite laminate reaches its individual failure criterion (e.g., Hashin, Tsai-Wu, or Puck). Although only one ply has failed, the FPF is often treated as the laminate’s failure for conservative design purposes.
Concept
The laminate consists of k plies, each carrying a different stress level depending on its fibre orientation.
When one ply fails (e.g., due to fibre breakage or matrix cracking), stress redistributes among the remaining intact plies.
In FPF analysis, this redistribution is not modelled — failure is assumed as soon as the first ply fails.
Details
Assumptions:
  The laminate fails when the first ply reaches its failure index = 1.
  No load sharing or stiffness degradation is considered.
Advantages:
  Simple and fast to implement.
  Suitable for preliminary design and analytical studies.
  Computationally efficient when compared to progressive models.
Limitations:
  Overly conservative — ignores remaining load-carrying capacity.
  Does not represent real structural behaviour beyond first damage.
  Cannot capture damage evolution or residual stiffness.
Use case:
  Appropriate for certification margins and initial sizing, where safety and simplicity are prioritised.
Key Takeaway
FPF = laminate failure onset (conservative).
Represents damage initiation, not complete structural collapse.
Valuable in design validation but must be complemented by Progressive Failure Analysis (PFA) for realistic damage-tolerant design.

## Slide 50: Laminate failure- Progressive Failure
Progressive failure analysis of a composite laminate examines the evolution of the load-displacement throughout the loading process up to ultimate failure event.
This approach is computationally expensive (material nonlinearity) and is implemented in Finite Element Analysis (FEA).
After FPF, the composite may still carry load and hence the load may be increased further.
Load increases until another ply fails, Second ply Failure (SPF).
The process carries on until all plies in the laminate fail accordingly and load drops.
Every time a ply fails, the laminate stiffness decreases.
This leads to reduction of load increase (slope).
Notes: Intro Progressive Failure Analysis (PFA) captures the entire damage evolution of a composite laminate — from initial ply cracking to final catastrophic failure. Unlike the conservative First Ply Failure (FPF) approach, PFA allows damaged plies to degrade in stiffness while intact plies continue to carry load.
Concept
PFA tracks the load–displacement behaviour of a laminate beyond the first damage event.
After the first ply fails, the remaining plies redistribute load based on reduced stiffness (degraded material properties).
The analysis continues through subsequent ply failures until the laminate can no longer sustain load.
Details
Stages of progressive failure:
  FPF (First Ply Failure): Damage initiates in the weakest ply.
  SPF (Second Ply Failure): Load redistributes and causes additional ply failure.
  Ultimate Failure: The laminate loses global load-carrying capacity.
Material degradation: Each failed ply contributes to stiffness reduction; this nonlinearity is handled in FEA through property degradation or element deletion techniques.
Computational aspects:
  Requires iterative stress re-evaluation after each failure.
  Computationally demanding due to nonlinear stiffness updates.
  Implemented in software such as Abaqus, Altair, and Ansys using user-defined subroutines (e.g., UMAT/VUMAT).
Interpretation of the Graph (Right Panel)
α₁ represents the initial stiffness slope before any damage.
α₂ shows reduced stiffness after ply failure (tan α₂ < tan α₁).
Each slope change reflects a stiffness degradation event.
The laminate reaches ultimate load when no further load increase is possible, signifying total failure.
Key Takeaway
PFA is a realistic but computationally intensive method.
It captures damage progression, stiffness degradation, and residual strength.
Ideal for certification-level FEA and structural durability predictions, especially for aerospace-grade CFRP laminates.

## Slide 51: Example
Compare maximum stress and maximum strain failure criteria considering the following input:

## Slide 52: Solution- Maximum stress vs. Maximum strain criterion
Ultimate stress is taken as minimum of 117 MPa and 35 MPa
Max. stress
Max. strain
The values differ by a factor of 3.43 and the fracture mode is reversed: longitudinal fracture in the one case and transverse in the other.
Notes: Intro Compare maximum stress vs maximum strain criteria for a UD ply loaded with a fixed stress ratio: and . Material data: .
Concept
Treat loading as a proportional path controlled by so .
Find the smallest that violates each criterion.
Max stress compares stresses to strengths. Max strain compares strains to strain allowables with orthotropic coupling.
Details
Maximum stress criterion
  Check: .
  Governing limits along the loading path:
    .
    .
  Smallest governs ⇒ failure at .
  Prediction: (transverse tension governs).
Maximum strain criterion
  Orthotropic strains (plane stress):
    .
    Reciprocity: .
    .
  Allowables: , .
  Solve:
    .
    .
  Smallest governs ⇒ failure at .
  Prediction: .
  Check shear: < (safe).
Why results differ
  Max stress ignores coupling.
  Max strain accounts for Poisson interactions; large induces negative transverse strain via , delaying the transverse strain limit.
Key Takeaway
With tension, maximum stress predicts early failure at (very conservative).
Maximum strain predicts failure much later at dominated by the longitudinal strain limit.
For proportional multiaxial loading, strain-based criteria can be markedly less conservative because they capture orthotropic coupling.
ChatGPT can make
Intro Compare maximum stress vs maximum strain criteria for a UD ply loaded with a fixed stress ratio: 𝜎_𝐿=12" " 𝜎_𝑇and 𝜏_𝐿𝑇=0. Material data: 𝑋_𝑡=1400" MPa"," " 𝑌_𝑡=35" MPa"," " 𝑆=70" MPa"," " 𝐸_𝐿=46" GPa"," " 𝐸_𝑇=10" GPa"," " 𝐺_𝐿𝑇=4.6" GPa"," " 𝜈_𝐿𝑇=0.31.
Concept
Treat loading as a proportional path controlled by 𝜎_𝑇=𝑠 so 𝜎_𝐿=12𝑠.
Find the smallest 𝑠that violates each criterion.
Max stress compares stresses to strengths. Max strain compares strains to strain allowables 𝑋_𝑡/𝐸_𝐿," " 𝑌_𝑡/𝐸_𝑇," " 𝑆/𝐺_𝐿𝑇with orthotropic coupling.
Details
Maximum stress criterion
  Check: ∣𝜎_𝐿∣≤𝑋_𝑡," "∣𝜎_𝑇∣≤𝑌_𝑡," "∣𝜏_𝐿𝑇∣≤𝑆.
  Governing limits along the loading path:
    𝜎_𝐿=𝑋_𝑡⇒𝑠=𝑋_𝑡/12=116.7" MPa".
    𝜎_𝑇=𝑌_𝑡⇒𝑠=35" MPa".
  Smallest 𝑠governs ⇒ failure at 𝑠=35" MPa".
  Prediction: 𝜎_𝑇=35" MPa"," " 𝜎_𝐿=420" MPa"(transverse tension governs).
Maximum strain criterion
  Orthotropic strains (plane stress):
    𝜀_𝐿=(𝜎_𝐿−𝜈_𝐿𝑇 𝜎_𝑇 )/𝐸_𝐿=(12𝑠−0.31𝑠)/𝐸_𝐿=11.69𝑠/𝐸_𝐿.
    Reciprocity: 𝜈_𝑇𝐿=𝜈_𝐿𝑇 " " 𝐸_𝑇/𝐸_𝐿=0.31⋅10/46=0.06739.
    𝜀_𝑇=(𝜎_𝑇−𝜈_𝑇𝐿 𝜎_𝐿 )/𝐸_𝑇=(1−12𝜈_𝑇𝐿 )𝑠/𝐸_𝑇=0.19131" " 𝑠/𝐸_𝑇.
  Allowables: 𝜀_𝐿𝑢=𝑋_𝑡/𝐸_𝐿=1400/46000=0.03043, 𝜀_𝑇𝑢=𝑌_𝑡/𝐸_𝑇=35/10000=0.00350.
  Solve:
    𝜀_𝐿=𝜀_𝐿𝑢⇒11.69𝑠/𝐸_𝐿=𝑋_𝑡/𝐸_𝐿⇒𝑠=𝑋_𝑡/11.69=∗∗119.7𝑀𝑃𝑎∗∗.
    𝜀_𝑇=𝜀_𝑇𝑢⇒0.19131𝑠/𝐸_𝑇=0.00350⇒𝑠=∗∗183.0𝑀𝑃𝑎∗∗.
  Smallest 𝑠governs ⇒ failure at 𝑠≈119.7" MPa".
  Prediction: 𝜎_𝑇≈119.7" MPa"," " 𝜎_𝐿≈1436" MPa".
  Check shear: 𝛾_𝐿𝑇=𝜏_𝐿𝑇/𝐺_𝐿𝑇=0< 𝑆/𝐺_𝐿𝑇(safe).
Why results differ
  Max stress ignores coupling.
  Max strain accounts for Poisson interactions; large 𝜎_𝐿induces negative transverse strain via 𝜈_𝑇𝐿, delaying the transverse strain limit.
Key Takeaway
With 𝜎_𝐿=12𝜎_𝑇tension, maximum stress predicts early failure at 𝜎_𝑇=35" MPa"(very conservative).
Maximum strain predicts failure much later at 𝜎_𝑇≈120" MPa"dominated by the longitudinal strain limit.
For proportional multiaxial loading, strain-based criteria can be markedly less conservative because they capture orthotropic coupling.
ChatGPT can make

## Slide 53: Solution- Cause of discrepancy
This contradiction lies in the misuse done to establish the relation between the values of the ultimate stresses and ultimate strains.
In practice these values would have to be determined respectively in the case of plane stresses and of plane strains.
The respective criteria which would then be deduced from them could be applied only to these schemes.
In this way the relations between ultimate stresses and strains would be more complex.

## Slide 54: Example
Consider an orthotropic layer whose characteristics at fracture are given by:
This layer is subjected to a tension in the direction .
Plot (first in Cartesian coordinates for , the tensile strength as a function of the angle of tension, using Hoffman criterion.
Plot in polar coordinates for , the tensile strength as a function of the angle of tension, using Hoffman criterion.
Notes: Intro
Goal: determine the uniaxial tensile strength of a UD ply loaded at angle using the Hoffman criterion.
Given allowables: MPa, MPa, MPa, MPa, MPa.
Output: in Cartesian and the polar repeat .
Concept
Rotate a remote axial stress by into ply axes .
Insert transformed stresses into Hoffman quadratic and solve for at failure.
Hoffman distinguishes tension vs compression through asymmetric coefficients so it is more realistic than Tsai-Hill for off-axis loading.
Details
Stress transformation for a uniaxial at angle :
Hoffman plane-stress form (single ply):
With for zero prestress and coefficients (tension–compression asymmetric):
Insert as linear functions of to get a quadratic in :
where
  Choose the positive root for tensile capacity:
  For plotting (Cartesian), sweep and evaluate .
  For the polar plot, place radially at angle and mirror to using orthotropic symmetry.
Sanity checks with given allowables:
  : , ⇒ (returns 1500 MPa).
  : , ⇒ (returns 90 MPa).
  gives strong reduction dominated by and via terms.
Key Takeaway
Workflow: transform stresses → plug into Hoffman → solve the quadratic for → plot.
Results recover on-axis strengths at and and predict a deep off-axis valley near controlled by shear and transverse allowables.
Compared with Tsai-Hill, Hoffman’s tension–compression asymmetry yields more conservative strengths in compression-affected orientations and is generally preferred for design screening.
Intro
Goal: determine the uniaxial tensile strength of a UD ply loaded at angle 𝜃using the Hoffman criterion.
Given allowables: 𝑋_𝑡=1500MPa, 𝑋_𝑐=1700MPa, 𝑌_𝑡=90MPa, 𝑌_𝑐=250MPa, 𝑆=80MPa.
Output: 𝜎_𝑥𝑢 (𝜃)in Cartesian (0≤𝜃≤𝜋/2)and the polar repeat (0≤𝜃≤2𝜋).
Concept
Rotate a remote axial stress 𝜎_𝑥by 𝜃into ply axes (1ⓜ,=𝐿" " 2=𝑇).
Insert transformed stresses (𝜎_11ⓜ,𝜎_22ⓜ,𝜏_12 )into Hoffman quadratic and solve for 𝜎_𝑥at failure.
Hoffman distinguishes tension vs compression through asymmetric coefficients so it is more realistic than Tsai-Hill for off-axis loading.
Details
Stress transformation for a uniaxial 𝜎_𝑥at angle 𝜃:
  𝑚=cos⁡𝜃," " 𝑛=sin⁡𝜃
  𝜎_11=𝜎_𝑥 𝑚^2
  𝜎_22=𝜎_𝑥 𝑛^2
  𝜏_12=𝜎_𝑥 𝑚𝑛
Hoffman plane-stress form (single ply):
𝐶_1 (𝜎_22−𝜎_22^′ ├ )┤^2+𝐶_2 (𝜎_11−𝜎_11^′ ├ )┤^2+𝐶_3 𝜏_12^2+𝐶_4 (𝜎_11−𝜎_11^′ )(𝜎_22−𝜎_22^′ )+𝐶_5 (𝜎_11−𝜎_11^′ )+𝐶_6 (𝜎_22−𝜎_22^′ )=1┤┤
With 𝜎_11^′=𝜎_22^′=0for zero prestress and coefficients (tension–compression asymmetric):
  𝐶_1=1/(𝑌_𝑡 𝑌_𝑐 )
  𝐶_2=1/(𝑋_𝑡 𝑋_𝑐 )
  𝐶_3=1/𝑆^2
  𝐶_4=−1/2 " ⁣" (1/(𝑋_𝑡 𝑋_𝑐 )+1/(𝑌_𝑡 𝑌_𝑐 ))
  𝐶_5=1/𝑋_𝑡 −1/𝑋_𝑐
  𝐶_6=1/𝑌_𝑡 −1/𝑌_𝑐
Insert 𝜎_11,𝜎_22,𝜏_12as linear functions of 𝜎_𝑥to get a quadratic in 𝜎_𝑥:
𝑎(𝜃)" " 𝜎_𝑥^2+𝑏(𝜃)" " 𝜎_𝑥−1=0
where
■(𝑎(𝜃)=" " &𝐶_2 𝑚^4+𝐶_1 𝑛^4+𝐶_3 𝑚^2 𝑛^2+𝐶_4 𝑚^2 𝑛^2@𝑏(𝜃)=" " &𝐶_5 𝑚^2+𝐶_6 𝑛^2 )
  Choose the positive root for tensile capacity:
𝜎_𝑥𝑢 (𝜃)=(−𝑏(𝜃)+√(𝑏(𝜃├ )┤^2+4𝑎(𝜃)┤ ))/2𝑎(𝜃)
  For plotting 0≤𝜃≤𝜋/2(Cartesian), sweep 𝜃and evaluate 𝜎_𝑥𝑢 (𝜃).
  For the polar plot, place 𝜎_𝑥𝑢radially at angle 𝜃and mirror to 2𝜋using orthotropic symmetry.
Sanity checks with given allowables:
  𝜃=0^∘⇒𝑚=1,𝑛=0: 𝑎=𝐶_2, 𝑏=𝐶_5⇒ 𝜎_𝑥𝑢≈𝑋_𝑡(returns 1500 MPa).
  𝜃=90^∘⇒𝑚=0,𝑛=1: 𝑎=𝐶_1, 𝑏=𝐶_6⇒ 𝜎_𝑥𝑢≈𝑌_𝑡(returns 90 MPa).
  𝜃=45^∘gives strong reduction dominated by 𝑆and 𝑌_𝑡via 𝑚^2 𝑛^2terms.
Key Takeaway
Workflow: transform stresses → plug into Hoffman → solve the quadratic for 𝜎_𝑥𝑢 (𝜃)→ plot.
Results recover on-axis strengths at 0^∘and 90^∘and predict a deep off-axis valley near 30^∘ " ⁣"−" ⁣" 60^∘controlled by shear and transverse allowables.
Compared with Tsai-Hill, Hoffman’s tension–compression asymmetry yields more conservative strengths in compression-affected orientations and is generally preferred for design screening.

## Slide 55: Solution
See file “Hoffman.xls” for detailed solution.
We need to solve equation of order 4 as below:

## Slide 56: Solution
See file “Hoffman.xls” for detailed solution.
The Cartesian graph looks like below:
Chart: Angle (deg)
| 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90
 | 1500 | 420.3964 | 217.4017 | 149.9584 | 119.0283 | 103.1883 | 95.1202 | 91.4768 | 90.2325 | 90

## Slide 57: Solution
The polar graph is shown here:
Chart: 
| 0 | 20 | 40 | 60 | 80 | 100 | 120 | 140 | 160 | 180 | 200 | 220 | 240 | 260 | 280 | 300 | 320 | 340
 | 1500 | 217.4017 | 119.0283 | 95.1202 | 90.2325 | 90.2325 | 95.1202 | 119.0283 | 217.4017 | 1500 | 217.4017 | 119.0283 | 95.1202 | 90.2325 | 90.2325 | 95.1202 | 119.0283 | 217.4017

## Slide 58: Example
For the previous example, compare the maximum stress failure criterion with that of Hoffman.
Notes: Concept
Rotate the remote axial stress by θ into the ply axes: .
Maximum stress: failure when any transformed component reaches its allowable. (tension case).
Hoffman: uses the quadratic with tension–compression asymmetry. With zero prestress: . Insert the transformed stresses → quadratic with . Tensile capacity: .
Details (quick numbers)
Using the given allowables, typical values are:
• Max-stress: MPa (fiber tension limit) • Hoffman: MPa (recovers )
• Max-stress: MPa (shear governs) • Hoffman: MPa
• Max-stress: MPa • Hoffman: MPa
• Max-stress: MPa (transverse tension governs) • Hoffman: MPa
• Max-stress: MPa (matrix tension limit) • Hoffman: MPa (recovers )
Key takeaways
Both criteria match the on-axis strengths at and .
Off-axis (≈30–60°), Hoffman predicts lower strength than maximum stress because it includes interaction terms and tension–compression asymmetry.
Maximum stress is simple and conservative by component, but it ignores interactions—it picks the smallest of .
Hoffman is generally preferred for design screening of off-axis tensile loading (more realistic), while maximum stress is useful for quick checks and bounding.
Concept
Rotate the remote axial stress 𝜎_𝑥by θ into the ply axes: 𝑚=cos⁡𝜃," " 𝑛=sin⁡𝜃 𝜎_11=𝜎_𝑥 𝑚^2," " 𝜎_22=𝜎_𝑥 𝑛^2," " 𝜏_12=𝜎_𝑥 𝑚𝑛.
Maximum stress: failure when any transformed component reaches its allowable. 𝜎_𝑥𝑢^"MS" (𝜃)=min⁡" ⁣" (𝑋_𝑡/𝑚^2 ," " 𝑌_𝑡/𝑛^2 ," " 𝑆/(∣𝑚𝑛∣))(tension case).
Hoffman: uses the quadratic with tension–compression asymmetry. With zero prestress: 𝐶_1=1/(𝑌_𝑡 𝑌_𝑐 )," " 𝐶_2=1/(𝑋_𝑡 𝑋_𝑐 )," " 𝐶_3=1/𝑆^2 ," " 𝐶_4=−1/2 " ⁣" (1/(𝑋_𝑡 𝑋_𝑐 )+1/(𝑌_𝑡 𝑌_𝑐 ))," " 𝐶_5=1/𝑋_𝑡 −1/𝑋_𝑐 ," " 𝐶_6=1/𝑌_𝑡 −1/𝑌_𝑐 . Insert the transformed stresses → quadratic 𝑎(𝜃) 𝜎_𝑥^2+𝑏(𝜃) 𝜎_𝑥−1=0with 𝑎=𝐶_2 𝑚^4+𝐶_1 𝑛^4+(𝐶_3+𝐶_4 ) 𝑚^2 𝑛^2, 𝑏=𝐶_5 𝑚^2+𝐶_6 𝑛^2. Tensile capacity: 𝜎_𝑥𝑢^"Hoff" (𝜃)=(−𝑏+√(𝑏^2+4𝑎))/2𝑎.
Details (quick numbers)
Using the given allowables, typical values are:
𝜃=0^∘ • Max-stress: 1500MPa (fiber tension limit) • Hoffman: ≈1500MPa (recovers 𝑋_𝑡)
𝜃=30^∘ • Max-stress: MPa (shear governs) • Hoffman: ≈𝟏𝟓𝟗MPa
𝜃=45^∘ • Max-stress: MPa • Hoffman: ≈𝟏𝟏𝟓MPa
𝜃=60^∘ • Max-stress: MPa (transverse tension governs) • Hoffman: ≈𝟗𝟖MPa
𝜃=90^∘ • Max-stress: 90MPa (matrix tension limit) • Hoffman: ≈90MPa (recovers 𝑌_𝑡)
Key takeaways
Both criteria match the on-axis strengths at 0^∘and 90^∘.
Off-axis (≈30–60°), Hoffman predicts lower strength than maximum stress because it includes interaction terms and tension–compression asymmetry.
Maximum stress is simple and conservative by component, but it ignores interactions—it picks the smallest of {𝑋_𝑡ⓜ,/ⓜ,𝑚^2 " " 𝑌_𝑡/𝑛^2 " " 𝑆/(𝑚𝑛) }.
Hoffman is generally preferred for design screening of off-axis tensile loading (more realistic), while maximum stress is useful for quick checks and bounding.

## Slide 59: Solution
Chart: Angle (deg)
| 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90
Hoffman | 1500 | 420.3964 | 217.4017 | 149.9584 | 119.0283 | 103.1883 | 95.1202 | 91.4768 | 90.2325 | 90
Max. Stress | 1500 | 468 | 249 | 185 | 162 | 153 | 120 | 102 | 93 | 90
Notes: Key takeaways
Trend matches theory: both curves meet at and at , and Hoffman is consistently more conservative off-axis because it includes interaction + tension/compression asymmetry.
Minimum region: the pronounced “valley” between ~30–60° is controlled by and the plot shows that clearly.
Relative gap: the green (Hoffman) should sit noticeably below the yellow (Max-Stress) around 30–60° — which it does.
Key takeaways
Trend matches theory: both curves meet 𝑋_𝑡at 0^∘and 𝑌_𝑡at 90^∘, and Hoffman is consistently more conservative off-axis because it includes interaction + tension/compression asymmetry.
Minimum region: the pronounced “valley” between ~30–60° is controlled by 𝑆 and 𝑌_𝑡; your plot shows that clearly.
Relative gap: the green (Hoffman) should sit noticeably below the yellow (Max-Stress) around 30–60° — which it does.